Impact of Fuel Rod Coatings on Reactor Performance and Safety

A Thesis Presented for the

Master of Science

Degree

The University of Tennessee, Knoxville

Ian Robert Stewart

May 2015

Acknowledgements

Foremost, I would like to thank my advisor and committee chair, Dr. Laurence F. Miller, for his support throughout this process. His patience and encouragement in the beginning proved to be vital in giving me a direction for my research.

I would also like to thank Dr. Ronald Pevey and Dr. Brian Wirth for being on my committee and giving me honest feedback when and where it was required. Their time and opinions were crucial to the completion of this thesis and my Master’s degree.

A sincere thanks for Dr. Kurt Sickafus for trusting me to present on my material on behalf of the NEUP project. Furthermore, none of this would be possible without the financial support from the Nuclear Energy University Program - Integrated Research Projects (NEUP-IRP).

Lastly, I want to thank my family and friends for helping shape me into who I am today.

Abstract

This study evaluates the use of a ceramic coating on the Zr-alloy cladding within a PWR using four ceramic compounds of 5 and 10 micron thicknesses: ZrO2, TiAlN, Ti2AlC, and Ti3AlC2. The film’s impact is assessed for variation on: reactivity, fuel cycle length, maximum temperature, film’s roughness, and transient conditions. The reactivity is analyzed using the following methods: change in the multiplication factor (k) each film introduces to the system using the ABH method, and Monte Carlo software (MCNP). Both methods are in good agreement, yielding less than half a percent change from a reference, no-film fuel pin. In order from lowest impact to highest impact on reactivity, the films are as follows for 10 micron thickness: ZrO2 (0.06%), TiAlN (0.20%), Ti3AlC2 (0.21%), and Ti2AlC (0.25%). This change directly impacts the fuel cycle length of the fuel. A linear reactivity model is used to approximate the loss in fuel cycle length and final burnup for a reference cycle of 300 days and 50 MWd/kg, respectively. The estimated loss in days is less than a day for all 5-micron films and less than 3 days for all 10 micron films (highest: 2.25 days, Ti2AlC) with all burnup calculations around 48.50 MWd/kg for all films. The impact the film yields on the temperature of the fuel pin is calculated using the one-dimensional thermal resistance circuit for each region (fuel, gap, clad, film, and moderator). The films’ thermal conductivity will directly impact this calculation, yet for the thin ceramic films, the percent change from a reference fuel is less 1% for all films at both thicknesses (largest change, lowest thermal conductivity: ZrO2). The roughness of the films currently being deposited is around 10 microinch Ra. This value is used with two perturbations, 5 microinches and 15 microinches, to evaluate the impact on the heat transfer coefficient and the induced friction-loss (pressure). For all roughness values the heat transfer coefficient stays well within typical PWR values while inducing a smaller pressure drop along the channel (compared to Zr-alloy clad). The thermal analysis is used to simulate a transient by varying the linear power density and the coolant flow rate. These two parameters are varied at different rates to impose a momentary mismatch in the system. In all simulations, the film reacts almost identical of that of the Zr-alloy clad reference model.

Table of Contents

1:  Introduction	1

2:  Methodology	3

2.1:  Reactivity / Multiplication Factor	3

2.2:  Fuel Cycle Length	9

2.3:  One-Dimensional Fuel Temperature	11

2.4:  Film Roughness	16

2.5:  Uncertainty Analysis	19

2.6:  Fuel and Coolant Temperature during Transients	23

3:  Results	26

3.1:  Reactivity Impact	26

3.2:  Loss in Fuel Cycle Length	30

3.3:  Fuel Maximum Temperature	31

3.4:  Film Roughness Impact	33

3.5:  Parameter Uncertainty Analysis	35

3.6:  Temperature Change during Flow Transient	37

4:  Conclusion	47

5:  Future Work	48

Works Cited	49

Appendix	51

Vita	65

List of Tables

Table 1: Triangular Distribution Parameters for an example uncertainty values for ZrO2 film	21

Table 2: Geometric parameters of reference fuel pin and coating	27

Table 3: Film properties	28

Table 4: Absorption cross section for proposed ceramic films	28

Table 5: Analysis of 5 micron and 10 micron thick film region with the ABH method	29

Table 6: Reactivity impact from 5 and 10 micron thick film	30

Table 7: Estimated loss fuel cycle length based on a 900 day cycle and fuel burnup.	31

Table 8: Parameters for the calculation of temperature changes in a fuel pin.	32

Table 9: Thermal conductivity of proposed coatings	32

Table 10: Impact on fuel centerline temperature for each film at 5 and 10-micron thickness.	33

Table 11: Physical properties of water coolant	34

Table 12: Impact on heat transfer coefficient with various film friction factors.	34

Table 13: Pressure drop induced by film roughness along the flow channel	35

Table 14: Uncertainty obtained for ABH method and centerline temperature.	36

Table 15: Multiplication factor and centerline temperature with uncertainty	37

Table 16: Depletion of each film isotope using constant power approximation equation.	54

Table 17: Isotropic Depletion using constant flux approximation equation	55

Table 18: Multiplication factor with varying boron concentration ratios at 10-micron film	56

Table 19: Multiplication factor for different boron concentration ratios at 100-micron film	56

Table 20: Reactor Information from Duderstadt text Appendix H	57

List of Figures

Figure 1: Five categories that require consideration for new fuel designs	2

Figure 2: Fuel geometry used in obtaining PMF.	7

Figure 3: Parameters used in ABH method	8

Figure 4: Linear Relationship of reactivity and burnup at a nominal initial reactivity	9

Figure 5: Reactivity vs. Burnup relationship obtained from the EPRI	10

Figure 6: Electrical circuit analogy for thermal resistance across a cylindrical fuel pin	11

Figure 7: Moody diagram illustrating relationship between friction factor, relative surface roughness, and flow parameters	17

Figure 8: Flow of a Monte Carlo simulation for ABH method to calculate the thermal utilization factor.	22

Figure 9: Monte Carlo simulation for fuel temperature calculation for the heat transfer coefficient and thermal conductivity of the film.	22

Figure 10: No-film region simulation illustrating the two varying parameters and the impact on the moderator temperature change along the channel.	39

Figure 11: Power transient followed by slower velocity change using 10μm ZrO2 film	40

Figure 12: Power transient followed by slower velocity change using 10μm TiAlN film.	41

Figure 13: Power transient followed by slower velocity change using 10μm Ti2AlC film.	41

Figure 14: Power transient followed by slower velocity change using 10μm Ti3AlC2 film.	42

Figure 15: Reference run for flow velocity variation followed by power density.	43

Figure 16: Flow velocity transient followed by slower power density change using 10μm ZrO2 film and lower heat transfer coefficient	44

Figure 17: Flow velocity transient followed by slower power density change using 10μm TiAlN film and lower heat transfer coefficient	44

Figure 18: Flow velocity transient followed by slower power density change using 10μm Ti2AlC film and lower heat transfer coefficient	45

Figure 19: Flow velocity transient followed by slower power density change using 10μm Ti3AlC2  film and lower heat transfer coefficient.	45

Figure 20: Depletion of a single isotope comparison using constant flux and constant power approximations.	52

# 1:  Introduction

The current fleet of light water reactors (LWRs) in the United States uses a UO2 fuel and a Zr-alloy, or Zircaloy, cladding material. The fuel element design and reliability is a key aspect to maintaining a safe, cost-competitive source of power. In order keep nuclear energy as a key component for power production in the future, continuous research and development is vital. The Nuclear Energy Research and Development Roadmap prepared by the United States Department of Energy (DOE) organizes the future challenges of the nuclear industry into four categories: [1]

“  1. develop technologies and other solutions that can improve the reliability, sustain

the safety, and extend the life of current reactors;

2. develop improvements in the affordability of new reactors to enable nuclear energy to help meet the Administration's energy security and climate change goals;

3. develop sustainable nuclear fuel cycles; and

4. understanding and minimization of risks of nuclear proliferation and terrorism. ”

With the recent nuclear accident suffered at the Fukushima Dai-ichi nuclear facility in March of 2011, renewed interest in fuel design has been brought to the forefront once again. During the events that occurred at the Fukushima Dai-ichi facility, the Zr-alloy cladding underwent severe oxidation reactions due to the high temperature water around the fuel, creating large amounts of hydrogen. [1,2]  From the lessons learned from the Fukushima Dai-ichi accident, alternative fuel and cladding concepts are being developed in order to enhance the safety of the reactor, competiveness, and economics of the current power reactor fleet. These new fuel/clad concepts is a part of the Accident Fuel Campaign and have been given the name Accident Tolerant Fuels (ATF) by the nuclear industry. The purpose of the ATFs is to increase the safety of the reactor system during beyond-design-basis accidents (e.g. loss of coolant accidents) and increase the time before fuel failure, all while improving, or remaining reasonably close to the conventional UO2-Zr, the system during normal operations (e.g. economics, reliability, spent fuel management).  To accomplish these tasks, various concepts have been proposed, such as: silicon-carbide clad, various iron-based alloys for clad, refractory materials, additional film region applied to Zr-clad, and numerous UO2 fuel replacements. [2,3]

This study evaluates an applied thin ceramic film to the moderator side of the Zr-clad within a PWR. This concept proposes an ATF notion that can be implemented in the currently operating reactors, with minimal design change required. This backward-compatibility is essential to implementing a new fuel design. The figure below illustrates the issues that must be addressed in order to employ a new fuel concept. [2,4]

### Figure 1: Five categories that require consideration for new fuel designs. [1]

This report addresses some of these considerations for various ceramic films at various thicknesses.

# 2:  Methodology

This study examines four ceramic films at thicknesses of 5 and 10 micron. The proposed films include:

- ZrO2,

- TiAlN,

- Ti2AlC, and

- Ti3AlC2.

The addition of a film region will introduce changes to the neutronic and thermal characteristics, of the fuel. In particular, impacts of these films on the following neutronic and thermal hydraulic operational and safety parameters are reported:

- Reactivity,

- Fuel Cycle Length,

- Fuel Centerline Temperature,

- Film roughness, and

- Impact on Fuel and Coolant Temperature during Transients.

Uncertainty analysis is implemented via Monte Carlo sampling techniques of uncertain parameters to illustrate the confidence of the calculations.

## 2.1:  Reactivity / Multiplication Factor

The addition of a ceramic film region to the moderator-side of the cladding will impact the neutron economy in the reactor. In terms of expressing the neutronic impact, this project evaluates the multiplication factor (k) which gives the ratio of number neutrons in one generation to the number of neutrons in the preceding generation. Moreover, we calculate the multiplication factor (k), assuming infinite medium (k∞), which can be expressed in a four-factor formula given in Equation 1 (neglecting leakage terms):[5]

k∞=ηfpϵ                                                            (Eq.1)

where, η is the reproduction factor, f  is the thermal utilization factor, p is the resonance escape probability, and ϵ is the fast fission factor. It is beneficial at this point to expand each term in the equation in order to understand the effect the ceramic film will induce on each: [5,6]

- Reproduction factor η: number of fission neutrons produced per absorption in the fuel, η=ν ( σfF/σaF )

- Thermal utilization factor f: ratio of the macroscopic cross sections of the fuel to the macroscopic of the fuel plus the remaining material in the core (i.e. probability that a thermal neutron is absorbed by the fuel), f=ΣaF/Σa

- Resonance escape probability p: fraction of fission neutrons that manage to slow down from fission to thermal energies without being absorbed

- Fast fission factor ϵ: ratio of the total number of fission neutrons (from both fast and thermal fission) to the number of fission neutrons from thermal fissions.

The ceramic film will have minor effects on the reproduction factor, resonance escape probability, and the fast fission factor. Therefore, further consideration in the thermal utilization factor is evaluated and, if we assume there is no change in the other three parameters in the four-factor formula, the thermal utilization will represent the impact the film has on the system. Directly, the thermal utilization change will yield the impact the film introduces on the neutron economy, and it can be expanded to illustrate how each region will present an impact:

f=ϕfuelΣabsfuelVfuelϕfuelΣfuelVfuel+ϕmodΣabsmodVmod+ϕΣVrest  ,                              (Eq.2)

where, ϕ represents the neutron flux in the respective region, Σabs is the absorption cross section, and V is the volume fraction. The other regions (e.g. gap, clad, film) can be lumped into the ϕΣVrest variable. However this method expressed in Equation 2 results in poor estimates changes of the thermal utilization due to adding a coating. [5,6]  An alternative analytical scheme based on transport theory proposed by Amouyal, Benoist, and Horowitz, referred to as the ABH method, is used to expand the thermal utilization factor. The ABH method uses an approximation of the probability that a neutron escaping the fuel will be absorbed in the moderator (βM) expressed in Equation 3: [5]

βM=VMVFΣabsMΣabsFPMFPF                                                   (Eq.3)

where, ΣabsF and ΣabsM represent the absorption macroscopic cross section for the fuel and moderator region respectively, VMVF represents the moderator to fuel volume fraction, PMF is the transfer probability characterizing source neutrons born in the moderator and absorbed in the fuel, and PFis the probability that a neutron born in the fuel escapes the fuel before being absorbed.

In order to obtain βM, the terms PMF and PF are required. Assuming a large (compared to mean free path), purely absorbing fuel lump, the PF can be approximated as [5]

PF≅SF4VFΣabsF                                                              (Eq.4)

where SF represents the surface area of the fuel region. Thus, βM can now be rewritten as

βM=4ΣabsMVMSFPMF.                                                       (Eq.5)

From Duderstadt text: Assuming that “all thermal neutrons first appear as a slowing down source uniformly distributed in the moderator, the thermal utilization is then just the probability characterizing source neutrons born in the moderator and absorbed in the fuel”, or PMF. [5]

f=PMF=VFVMΣabsFΣabsMPFM                                              (Eq.6)

Where, PFM describes the probability that a neutron born in the fuel will eventually be absorbed in the moderator region. [5] This probability is expressed as the product of the βM and PF, the probability that a neutron in the fuel will be eventually absorbed in the fuel.

PFM=PF βM                                                           (Eq.7)

Combining Equations 5 and 6, we obtain a new equation for the thermal utilization factor. [5]

f=VFVMΣabsFΣabsMPF βM                                                  (Eq.8)

Equation 7 can then be rewritten using Equation 4 and 5:

1f-1=ΣabsMΣabsFVMVF1PF+1-PMFPMF-4ΣabsMVMSF                          (Eq.9)

The key idea involved in the ABH method is obtaining a crude scheme to obtain PMF. This is accomplished by using diffusion theory with transport-corrected boundaries between the fuel-moderator regions. [5] This is achieved by solving Equation 10

DM∇2ϕMr-ΣabsMϕMr=-q0                                (Eq.10)

and using the boundary conditions:

dϕMdr r=b=0     ,                                         (Eq.11)

1ϕMdϕMdr r=a=1d     ,                                         (Eq.12)

where DM is the diffusion coefficient in the moderator region, ϕM is the flux within the moderator, q0 is the linear power density, d is a transport boundary correction, and a/b are radial values from Figure 2. [5,6]

### Figure 2: Fuel geometry used in obtaining PMF.

Assuming PMF~PM, we need to solve for PM.

PM=2πaDMq0VMdϕMdra                                             (Eq.13)

Sparing the details of solving the diffusion equation and the PM probability, the final result is given by

PM=VMad2VFLM2+EaLM,bLM-1≅PMF                          (Eq.14)

where LM2=DM/ΣabsM and E(…) is the lattice function, which in this case will be in cylindrical form. [5] Combining the equations, we arrive at the final expression of the ABH method:

1f=ΣabsMVMΣabsFVF1+ΣabsFΣtotF1-PFOPFO-aΣtotF1+aΣsFΣtotF+βΣsFΣtotF2+  ad2LM2-aΣaMVMVF+E aLM,bLM     ,                                                                                                    (Eq.15)

where α and β are parameters for cylindrical geometries given in Figure 3. [5]

### Figure 3: Parameters used in ABH method. [5]

To confirm the results from the ABH method, Monte-Carlo N-Particle (MCNP) software code developed at Los Alamos National Laboratory is also utilized to determine the reactivity effects of the coatings on a fuel pin. The MCNP code can be used for particle transport and for eigenvalue calculations (e.g. keff) for numerous scenarios. In this study, a single, one-dimensional fuel rod (infinite in length) is used with five regions: fuel, gap, cladding, film, and moderator. Within MCNP, the KCODE card is implemented to solve for the keff eigenvalue (example problem in Appendix). [7]

## 2.2:  Fuel Cycle Length

To approximate the impact on isotope depletion, the production chains for the principal isotopes (e.g. =Uranium 235), neutron flux, and reactivity calculations must be coupled. A variation in reactivity due to the film will directly affect the refueling schedule of the reactor. Thus, it is vital to evaluate the impact on the fuel cycle length in order to examine the economic performance of a reactor. In order to assess fuel burnup and loss in fuel cycle length a linear reactivity model is used to estimate impact of changes in initial reactivity on burnup. Reactivity (ρ) loss as a function of burnup (B) becomes fairly linear after a few months of operation for a reactor, as is illustrated by Figure 4. [8]

### Figure 4: Linear Relationship of reactivity and burnup at a nominal initial reactivity. [8]

The change in reactivity previously obtained using the ABH method and MCNP can be used to approximate the burnup of the fuel. That is, one can multiply the percent loss in reactivity by an initial fuel cycle length value. Figure 5 from the Linear Reactivity Model for Nuclear Fuel Management text illustrates the linear estimate using a 300 days fuel cycle at 4.34 wt% enrichment supplied via Electric Power Research Institute (EPRI) [8].

### Figure 5: Reactivity vs. Burnup relationship obtained from the EPRI. [8]

The red-line in Figure 5 is added to illustrate the change in reactivity and the impact on the burnup for a reference reactor. In this study, this linear reactivity model is used to assess the loss in fuel cycle length for a 900 day cycle (i.e. three periods of 300 days within the reactor) and the final burnup value based on a reference burnup of 50 MWd/kg. The loss in fuel cycle length (days) and final burnup value is obtained from the reactivity change from a regular (no-film region) fuel pin.

## 2.3:  One-Dimensional Fuel Temperature

The addition of a ceramic film will affect the heat transfer between the fuel and moderator, thus changing the maximum fuel temperature. It is crucial to verify that the maximum fuel temperature, or in this case the fuel centerline temperature, remains within a safe region. In this study, the overall thermal resistance of a fuel pin is used to evaluate the temperature drop from the fuel centerline to the coolant. This task can be accomplished by using a circuit analogy of a series of thermal resistances for each region: fuel, gap, cladding, ceramic film, and coolant. Figure 6 from Todreas illustrates the temperature profile for the five regions: [6]

### Figure 6: Electrical circuit analogy for thermal resistance across a cylindrical fuel pin. [6]

where Tmax or TCL is the centerline temperature, Tfo is the outer surface temperature of the fuel, Tci is the inside surface cladding temperature, Tco is the outer surface temperature of the cladding, Too is the outer ceramic film temperature, and Tm is the moderator temperature.

Now, we must derive the unique heat transfer equations for each region. Starting in the fuel region, the heat conduction equation for a cylindrical fuel pellet with a uniform volumetric heat source q''' and ignoring axial heat conduction takes the form: [5,6]

1rddrkF rdTdr=-q'''                                                   (Eq.16)

where r is the position radius, kF is the thermal conductivity of the fuel, and T is temperature. To simplify the equation, we consider a constant thermal conductivity and no dependency on position or temperature, thus ddrkF=0. Now we are able to solve for the temperature drop across the fuel pin (dT/dr): [6]

dTdr=TCL-q'''r24 kF .                                                    (Eq.17)

We can define this function in terms of linear power density q', yielding a new form of the previous equation:

q'=πrF2q'''                                                      (Eq.18)

ΔTF=q'4π kF                                                         (Eq.19)

Note that this form is based on the assumption that fuel temperature is only dependent on the fuel’s thermal conductivity and the linear power density, and not the fuel radius. [5,6]

Second region is the gap between the fuel pellet and the cladding. This region has a tight clearance between the fuel and cladding with values around 0.008 cm and usually filled with an inert gas (e.g. helium) for LWRs. [5] Without going through a full derivation of the heat equation, similar to the equation for the fuel region (except no heat production), we can show the final form of the equation for the temperature drop across the gap as: [5,6]

ΔTG=q''hG                                                         (Eq.20)

where, hG is the heat transfer coefficient in the gap region and the heat flux q'' across the gap region is the amount of heat produced from the fuel divided by the surface area of the fuel region. That is, in terms of heat flux, the equation takes the form:

q''=q'''πrG2H2πrGH=q'''rG2=q'2πrG  ,                                    (Eq.21)

then combining the equations to obtain the final equation for temperature drop across the gap: [5,6]

ΔTG=q'''rG2hG=q'2πrGhG .                                             (Eq.22)

The third region of the fuel pin is the cladding. This region, like the gap, has no heat production term, thus we are able to solve the temperature drop fairly easily. The heat conduction equation takes the form [6]

1rddrkC rdTdr=0 .                                                  (Eq.23)

Sparing the details, we are able to find the temperature drop across the clad: [5,6]

ΔTC=q'''rC2tCkC=q'2π rCtCkC   ,                                     (Eq.24)

where kC represents the thermal conductivity of the clad and tC is the clad thickness.

The fourth region is the ceramic film. The temperature drop across the film, like the gap and cladding, is dependent on the thermal conductivity and the thickness of the film. Assuming no heat production from the film, the heat conductivity equation can be solved to obtain a temperature profile across the film: [6]

ΔTfilm=q''tfilmkfilm=q'2π tfilmrfilm kfilm ,                                     (Eq.25)

where tfilm is the film thickness, rfilm is the distance to the outside of the film, and kfilm is the thermal conductivity of the film region.

The last region is the moderator region. The heat flux leaving the fuel pin and emerging into the moderator region is given by:

qpin''=hsTfilm-TM ,                                               (Eq.26)

where hs is the heat transfer coefficient between the film-moderator region (dependent on flow conditions), Tfilm is the outer temperature of the ceramic film, and TM is the moderator temperature. The temperature drop from the film to the moderator is obtained by solving the previous equation for Tfilm-TM :

Tfilm-TM=q''hs=rfuel2 q'''hs 2rfilm=q'2π rfilmhs  .                             (Eq.27)

Note that normal notation for uses the difference between surface temperature and the coolant/moderator temperature. In this case, the film’s outer surface is the surface temperature. Now the overall thermal resistance equation can be found by adding each of the regions: [5,6]

TCL-TM=q'2π12kFuel+1rghg+tCrCkC+tfilmrfilm kfilm+1rfilmhs  .             (Eq.28)

The linear power density and moderator/coolant temperature will change along the length of the channel. We can assume that the linear power density has a sine-like shape along the length of the flow channel: [5]

q'z=q0'sinπzH .                                                 (Eq.29)

Then we can compute the coolant temperature along the channel by using a simple energy balance equation gained by the coolant from the fuel:

wcpdT=q''2πrFdz=q'zdz                                     (Eq.30)

where w is the mass flow, cp is the specific heat of the coolant, and z is the position along the channel. Using this form, we can integrate the up the flow channel from inlet to outlet (temperature and position): [5]

wcpTinletTMdT=q0'0zdz'sinπz'H  .                                  (Eq.31)

Solving this equation, we can calculate the temperature of the coolant at position z along the channel: [5]

TMz-Tinlet=q0'Hπcpw1-cosπzH  .                                (Eq.32)

Inserting the position dependent linear power density and moderator temperature into the overall thermal resistance equation: [5,6]

TCL=Tinlet+q0'Hπcpw1-cosπzH+q0'sinπzH2π12kFuel+1rghg+tCrCkC+tfilmrfilm kfilm+1rfilmhs.   (Eq.33)

Each of the proposed films will have a unique thermal conductivity, thus each film will affect the system uniquely, along with any film thickness variation (i.e. rfilm ,  tfilm ,  kfilm).

## 2.4:  Film Roughness

To further assess the impact the ceramic film yields on the system, the roughness of the film itself must be considered. This roughness, or friction, between the film-moderator will affect the heat transferred between the pin and the moderator, as well as present a pressure drop along the flow channel. [9] In order to evaluate the change in the heat transfer coefficient h and the pressure drop, the Moody diagram is used to obtain the Darcy friction factor f for various experimental roughness values. The Moody diagram relates flow parameters (e.g. Reynolds number, Re) and the roughness of the material to the Darcy friction factor. The Darcy friction factor is used in fluid dynamics to relate pressure drop produced by the friction between the wall of a pipe and the fluid flow. [6,9]

### Figure 7: Moody diagram illustrating relationship between friction factor, relative surface roughness, and flow parameters. [9]

The relative roughness is defined as the average roughness divided by the diameter of the cylinder. The average roughness used in this study is the arithmetic average of absolute values, denoted as Ra. [9] The actual values for the films’ roughness will be discussed later.

The roughness of film will produce a head loss due to the friction effects along the wall, or in our case, the outside of the fuel pin. Along the flow channel, the film induces a shear stress on the flow which decreases the fluid motion. [9] For steady-state, steady-flow conditions, the energy equation of the fluid can be written as

P1ρg+v122g+z1=P2ρg+v222g+z2+hf ,                                    (Eq.34)

where the subscript denotes the position along the cylindrical channel, P is pressure, ρ is the density of the fluid, v is the flow velocity, g is gravity, z is position along the channel, and hf is the head loss due to wall friction. Solving this equation for a given channel length L and same flow velocity along the channel, we can obtain an equation for pressure loss as a function of the Darcy friction factor:

ΔP=ρgfLdhv22g                                          (Eq.35)

where dh represents the hydraulic diameter. [6,9]

With the aim of evaluating the impact on the heat transfer coefficient the film roughness introduces, the Prandtl and Nusselt number are required. The Prandtl (Pr) number is the ratio of molecular diffusivity of momentum to that of heat in the fluid and is required to obtain the Nusselt number. The Nusselt (Nu) number expresses the ratio of convection to conduction heat transfer across a boundary. The equations for Pr and Nu are as follows:

Pr=μ cpk                                                    (Eq.36)

where, μ is the dynamic viscosity, cp is the specific heat, and k is the thermal conductivity of the fluid;

Nu=h dhk                                                  (Eq.37)

where, h is the heat transfer coefficient. [9]

In order to evaluate the film’s roughness impact directly, an alternate form of the Nusselt number is obtained using the Darcy friction factor. A correction by Gnielinski is given to correlate turbulent flow in tubes between the Reynolds (Re) number, Prandtl (Pr) number, and friction factor f is given: [6]

Nu=f/8Re*Pr1+12.7f/8Pr2/3-1 .                                      (Eq.38)

The Gnielinski correlation is valid for: [9]

0.5≤Pr≤2000

3000≤Re≤5E6 .

Now, one is able to obtain a value for the heat transfer coefficient by solving the original Nusselt equation:

h=Nu  kdh                                                (Eq.39)

This study will evaluate the change in the heat transfer coefficient under various flow conditions and several roughness values.

## 2.5:  Uncertainty Analysis

To obtain more knowledge regarding the impact the film presents on the system, uncertainty analysis is vital. The uncertainty in these calculations arises due to lack of knowledge in certain parameters. In this study, the uncertainty of the ABH method used to evaluate the thermal utilization and the temperature change across a fuel pin are analyzed. For each of the respective equations, the variables where the uncertainty is addressed are as follows:

ABH Method:  PFO (first-flight escape probability) and  ΣabsM

Temperature Change: hs (heat transfer coeff. between film-moderator) and kfilm

Regarding the ABH method parameters, the first-flight escape probability expresses the probability that a neutron born in the fuel will make its next collision in the moderator. With the of a ceramic film, the probability should decrease due to the film introducing its own probability of collision. The moderator’s absorption cross-section is lumped with the film’s volume-weighted absorption cross-section. Coupling this parameter with a certain uncertainty illustrates the impact the film might introduce.

For the temperature calculation, the heat transfer coefficient between the coolant-film and the (approximated) thermal conductivity of the film are both given values of uncertainty due to lack of information and author’s estimations for both parameters.

For the above parameters, a triangular distribution model is used to exhibit the variability. In order to properly assess the lowest, highest, and peak values for the triangular model, estimated perturbations are used with respect to each variable. The perturbation values will be discussed later within the Results section.

Using the probability distributions to obtain the lowest and highest values in the triangular distribution, Monte Carlo techniques are employed to acquire values from each of the probability functions. Monte Carlo sampling relies on repeated random sampling from these inputted triangular distributions resulting in a converged solution. @Risk software is implemented to analyze both temperature change and the ABH method for the given input distributions. This software performs risk analysis using Monte Carlo simulations within Microsoft Excel. By running the simulation numerous times (e.g. 1E6 histories), an output distribution of solutions is obtained. [10]

In order to properly assess the lowest, highest, and peak values for the triangular model, estimated perturbations are used with respect to each variable.

ABH Method:

PFO with 10% perturbation

ΣabsM with 20% perturbation

Centerline Temperature:

hs with 15% perturbation

kfilm with 20% perturbation

Table 1 contains numerical values of the uncertainty using ZrO2 film.

#### Table 1: Triangular Distribution Parameters for an example uncertainty values for ZrO2 film.

|  | ABH Method |  | Centerline Temperature |  |  |
| --- | --- | --- | --- | --- | --- |
| Parameter | PFO | ΣabsMod * | hs |  | kfilm* |
| Minimum | 0.4 | 0.16 | 2.4 |  | 1.6 |
| Most Likely | 0.5 | 0.22 | 3.0 |  | 2.0 |
| Maximum | 0.6 | 0.28 | 3.6 |  | 2.4 |

The asterisks on the macroscopic absorption cross-section and the thermal conductivity of the film in Table 1 indicate the parameters will change for each film. Furthermore, the film’s thickness will also impact the moderator absorption cross section (i.e. film’s cross section is added to the moderator region). Figures 8 and 9 illustrate the basic methodology for the Monte Carlo simulations for the ABH method and the fuel centerline temperature, respectively, with an example reference output from @Risk.

### Figure 8: Flow of a Monte Carlo simulation for ABH method to calculate the thermal utilization factor.

### Figure 9: Monte Carlo simulation for fuel temperature calculation for the heat transfer coefficient and thermal conductivity of the film.

To verify the results from @Risk, MATLAB is used. Employing the previous MATLAB codes used to calculate the thermal utilization (ABH method) and temperature change, the probability functions are entered for each of the parameters, respectively. The calculations result in a distribution of solutions with a computed variance and standard deviation.

## 2.6:  Fuel and Coolant Temperature during Transients

Using the overall thermal resistance equation, we can set a time dependent equation for various parameters in order to understand how the film will impact certain transient conditions. This study evaluates variable flow and variable (linear) power density while retaining a predetermined moderator temperature change ΔTM along the channel. Both time dependent equations are given an exponential decay. For this analysis, the values (i.e. flow rate and power density) are decreased exponentially to one-half of the original value. The general form for a given function ft is given by:

ft=12f0exp-λ t+1   ,                                              (Eq.39)

where t is response time and λ is a value given to the slope of change (i.e. how quickly the exponential change will occur, or exponential decay value). Using the two parameters we wish to assess, two equations are formed with the same form:

q't=12q'0exp-λ1t+1  ,                                               (Eq.40)

vt=12v0exp-λ2t+1  .                                               (Eq.41)

Thus, the product of the eigenvalue and time yield the response time of the varying parameter. That is, by varying the mass flow faster than the linear power density (i.e. λ2>λ1) will produce a momentary increase in coolant temperature. In this study, both mass flow and linear power density are varied by unique values (λ1,2) and compared to changes in a regular (no-film) fuel pin. For example, by assuming the exponential term is equal to a value, on can solve for the decay constant.

R1,2=exp-λ1,2 t ,                                                           (Eq.42)

One can obtain an equation for λ1,2:

λ1=lnR1t1 ,                                                           (Eq.43)

λ2=lnR2t2 ,                                                           (Eq.44)

where t1,2 represent the response times and R1,2 yield the slope of the exponential decay for each equation, respectively. In this study we use response time values (t1,2) of 60 seconds and 25 seconds with identical R1,2 values set to 0.5.

The flow velocity directly impacts the mass flow of the flow channel. This expression is given by:

mt=vtAcsρ ,                                                  (Eq.45)

for Acs is the cross-sectional area of the channel with a moderator density of ρ.

Combining the two time-dependent equations with the thermal resistance equation, we obtain:

TCL=Tinlet+ 12q'0exp-λ1t+1Hπcpmt1-cosπzH+ 12q'0exp-λ1t+1sinπzH2π(12kFuel+1Rghg+…

1kCladln RcoRci +δoRookfilm+1Rooh )  .                                         (Eq.46)

This equation is implemented using MATLAB software for all proposed films and compared with a reference, no-film pin.

# 3:  Results

## 3.1:  Reactivity Impact

Several parameters in the final expression of the ABH method previously derived are changed due to the addition of a coating. The addition of the coating region will slightly lower the moderator volume (dependent on film thickness), consequently decreasing the moderator-to-fuel volume fraction VMVF slightly (~0.40% decrease for 10 micron film). The volume of the moderator is obtained via subtracting the fuel, gap, clad, and film volumes from the squared pitch. If we assume a one centimeter depth, we can use the cross sectional areas to obtain a volume for each region. That is,

Area total=Pitch2=πrM2                                             (Eq.47)

then moderator volume-fraction can be obtained by

VM*=Pitch2- πrF+rgap+rclad+rfilm2Pitch2  ,                                 (Eq.48)

where rF, rgap, rclad, and rfilm are the radius values to the fuel, gap, clad and film region, respectively (the asterisk* on the moderator volume indicates the new value due to the film region).

The film will also introduce a higher absorption rate outside of the fuel region; therefore the absorption cross-section of the film is combined with the moderator cross section in the ABH equation. The cross section of the film is volume-averaged with the moderator cross section to obtain a new overall moderator absorption cross-section. The new moderator cross-section and new fuel diameter impact the lattice function through the LM variable (i.e. recall, LM=DM/ΣabsM) and the fuel boundary condition a, see Figure 3. The new moderator cross section takes the form of

ΣabsM*=VMVM+VfilmΣabsM+VfilmVM+VfilmΣabsfilm .                                 (Eq.49)

The final expression of the ABH method with the film present is shown where each parameter that is affected is given an asterisk *:

1f=ΣabsM*VM*ΣabsFVF1+ΣabsFΣtotF1-PFOPFO-a*ΣtotF1+αΣsFΣtotF+βΣsFΣtotF2+ a*d2LM2*-a*ΣabsM*VM*VF+                        E a*LM*,bLM*   .                                                 	                            (Eq.50)

This study assesses a Westinghouse PWR with the fuel pin dimensions summarized in 2. [5]

#### Table 2: Geometric parameters of reference fuel pin and coating.

| Parameter | Variable | Value |
| --- | --- | --- |
| Fuel Radius | rfuel | 0.4095 cm |
| Gap Thickness | tgap | 0.0082 cm |
| Clad Thickness | tclad | 0.0572 cm |
| Coating Thickness | tfilm | 5 or 10 micron |
| Fuel Element Pitch | Pitch | 1.25 cm |

Next, the absorption cross section for each film is required. The absorption macroscopic cross section is evaluated in Equation 50:

Σabs=Nσabs                                                         (Eq.51)

where, N represents the number density and σabs is the absorption microscopic cross section.

The number density, represented in Equation 51, represents the number of atoms per volume:

N=ρ*NAVM                                                           (Eq.52)

where, ρ is the film density, NAV is Avogadro’s number, and M is the molecular weight. The required data to obtain the macroscopic cross section for each film is presented in Table 3. [11,12,13]

#### Table 3: Film properties.

| Film | σabs (b) | Atomic Weight (g/mole) | Density (g/cc) |
| --- | --- | --- | --- |
| TiAlN | 7.921 | 88.888 | 3.86 |
| ZrO2 | 0.1854 | 123.22 | 6.00 |
| Ti2AlC | 11.845 | 134.791 | 4.10 |
| Ti3AlC2 | 17.649 | 194.702 | 2.93 |

Using these equations, the macroscopic absorption cross section (i.e. for n,γ reactions) can be obtained for each film.

#### Table 4: Absorption cross section for proposed ceramic films.

| Film | Σabs (cm-1) |
| --- | --- |
| TiAlN | 0.2074 |
| ZrO2 | 0.0054 |
| Ti2AlC | 0.1180 |
| Ti3AlC2 | 0.1601 |

To calculate the thermal utilization from the ABH method, MATLAB program is implemented to acquire values for each film, as well as a reference, no-film pin. The percent change from the reference is shown in Table 5 (See Appendix for MATLAB code).

#### Table 5: Analysis of 5 micron and 10 micron thick film region with the ABH method.

| Simulation | Film Thickness (micron) | Thermal Utilization | % Change |
| --- | --- | --- | --- |
| Reference | - | 0.8847 | - |
| ZrO2 | 5 | 0.8844 | 0.03% |
| TiAlN | 5 | 0.8832 | 0.14% |
| Ti2AlC | 5 | 0.8833 | 0.15% |
| Ti3AlC2 | 5 | 0.8837 | 0.11% |
| ZrO2 | 10 | 0.8842 | 0.05% |
| TiAlN | 10 | 0.8821 | 0.27% |
| Ti2AlC | 10 | 0.8820 | 0.30% |
| Ti3AlC2 | 10 | 0.8827 | 0.22% |

The change differs for each film due to unique values of density, which in return affects the absorption macroscopic cross section (i.e. through the number density) and the film’s microscopic absorption cross section. To compare as well as validate the change in reactivity via the ABH method, MCNP code is implemented. Using an infinite cylinder (i.e. infinite in length/height), a multiplication factor was calculated for each film as well as a reference fuel pin (See Appendix for MCNP input deck). A single fuel pin is used in the MCNP geometry with white boundaries on the outer boundary of the moderator. The multiplication factor (KCODE) calculation is performed using 1000 cycles and 1000 histories per cycle. The output k-value from MCNP is shown in Table 6 together with the previous ABH method values.

#### Table 6: Reactivity impact from 5 and 10 micron thick film.

|  |  | MCNP |  | ABH Method |
| --- | --- | --- | --- | --- |
| Simulation | Thickness (micron) | k-value | % change | % change |
| Reference | - | 1.49032 | - | - |
| ZrO2 | 5 | 1.48961 | 0.05% | 0.03% |
| TiAlN | 5 | 1.48768 | 0.18% | 0.14% |
| Ti2AlC | 5 | 1.48879 | 0.10% | 0.15% |
| Ti3AlC2 | 5 | 1.48948 | 0.06% | 0.11% |
| ZrO2 | 10 | 1.48936 | 0.06% | 0.05% |
| TiAlN | 10 | 1.48741 | 0.20% | 0.27% |
| Ti2AlC | 10 | 1.48654 | 0.25% | 0.30% |
| Ti3AlC2 | 10 | 1.48716 | 0.21% | 0.22% |

The keff values are well above the typical 1.0 values due to the white boundary inputted within MCNP. That is, the neutrons are reflected on the outside of the moderator region boundary, thus increasing the probability of being absorbed back in the fuel. Additionally, these calculations are coupled with a corresponding uncertainty analysis.

## 3.2:  Loss in Fuel Cycle Length

The change in reactivity or keff is used to approximate the impact on the fuel cycle length via the linear reactivity model. To assess the change in fuel cycle length, the reactivity change obtained from the MCNP simulations is used to estimate the loss in fuel cycle length and total burnup of the fuel. In this study, it is assumed a fuel element is in the reactor for three cycles of 300 days (i.e. 900 days total) and a reference burnup value of 50 MWd/kg is used, where a decrease in reactivity will directly impact the fuel cycle length. The loss in days of the fuel cycle  and the corresponding burnup is presented in Table 7.

#### Table 7: Estimated loss fuel cycle length based on a 900 day cycle and fuel burnup.

| Film | Thickness (micron) | Reactivity Change MCNP | Cycle Loss Estimate (days) | Burnup (MWd/kg) |
| --- | --- | --- | --- | --- |
| ZrO2 | 5 | 0.05% | 0.45 | 48.6 |
| TiAlN | 5 | 0.18% | 1.62 | 48.5 |
| Ti2AlC | 5 | 0.10% | 0.90 | 48.6 |
| Ti3AlC2 | 5 | 0.06% | 0.54 | 48.6 |
| ZrO2 | 10 | 0.06% | 0.54 | 48.5 |
| TiAlN | 10 | 0.20% | 1.80 | 48.5 |
| Ti2AlC | 10 | 0.25% | 2.25 | 48.4 |
| Ti3AlC2 | 10 | 0.21% | 1.89 | 48.5 |

The fuel length impact may be of primary interest for utilities, due to the reactor not creating power and to increasing the rate of refueling. In order to achieve the same fuel cycle, the fuel enrichment can be increased. For the 10 micron thick films, the fuel cycle impact is over two days for three of the films (TiAlN, Ti2AlC, Ti3AlC2), with largest fuel cycle loss of 2 days for the 10 micron Ti2AlC which may be of concern. The films decrease the total burnup to around 48.5 MWd/kg, a decrease of 1.5 MWd/kg from the reference case from the text at 4.34 wt%. [8]

## 3.3:  Fuel Maximum Temperature

Adding coatings to the fuel pin should increase the fuel centerline temperature by increasing the thermal conduction path a small amount; however, they may have a higher heat transfer coefficient than the cladding and consequently lower the fuel centerline temperature.  A rough estimate of this change is obtained based on typical PWR values listed in Tables 8 and on estimates for thermal conductivities listed in Table 9. [5,11,12,13] It should be noted that in this study the maximum linear power density is used to validate that the fuel will remain in a safe temperature region.

#### Table 8: Parameters for the calculation of temperature changes in a fuel pin.

| Parameter | Variable | Value |
| --- | --- | --- |
| Linear Power Density (Maximum) | qmax' | 460 W/cm |
| UO2 Fuel Thermal Conductivity | kFuel | 0.0250 W/cm-K |
| Clad (Zircaloy IV) Conductivity | kClad | 0.1070 W/cm-K |
| Heat transfer coefficient in gap | hGap | 0.75 W/cm2-K |
| Heat transfer coefficient in moderator | h | 3.0 W/cm2-K |
| Inlet Moderator Temperature | TMod | 290 ͦC |

#### Table 9: Thermal conductivity of proposed coatings.

| Coating | Thermal Conductivity (W/m-K) |
| --- | --- |
| ZrO2 | 2.0 |
| TiAlN Ti2AlC | 5.0 30.0 |
| Ti3AlC2 | 40.0 |

The thermal conductivity characterizes the film’s ability to transfer heat. That is, a smaller thermal conductivity yields a lower heat transfer rate through the film; thus, resulting in a higher fuel temperature compared to the high thermal conductivity films. Using the thermal resistance equation previously derived, the change in the maximum temperature can be calculated.

#### Table 10: Impact on fuel centerline temperature for each film at 5 and 10-micron thickness.

| Film | Thickness (micron) | Centerline Temperature °C | Change in TCL % |
| --- | --- | --- | --- |
| Reference | - | 1834.80 | - |
| ZrO2 | 5 | 1840.89 | 0.33% |
| TiAlN | 5 | 1837.22 | 0.13% |
| Ti2AlC | 5 | 1835.18 | 0.02% |
| Ti3AlC2 | 5 | 1835.07 | 0.02% |
| ZrO2 | 10 | 1847.01 | 0.67% |
| TiAlN | 10 | 1839.66 | 0.27% |
| Ti2AlC | 10 | 1835.58 | 0.04% |
| Ti3AlC2 | 10 | 1835.38 | 0.03% |

The centerline temperature is constrained to remain below the melting temperature of the fuel ~2800°C, [5] and the calculated fuel centerline temperatures for each simulation are well below the melting point of the fuel. This study used a one-dimensional thermal analysis, thus neglecting any axial conductance, as well as analyzing only a single fuel pin. The significance of these simulations is the percent changes each film introduces on the centerline temperature. Due to the small thickness values proposed of 5 and 10-microns coupled with a low thermal conductivity film introduces a slight increase with the largest increase in temperature (10-micron ZrO2 film) from the reference is 0.67% 12.21°C.

## 3.4:  Film Roughness Impact

To illustrate the impact the film’s roughness presents on the system, change in the heat transfer coefficient is analyzed under normal flow parameters. For reference and comparison, typical heat transfer coefficient values for Zr-clad to Water ranges from 2.8 – 4.5Wcm2 K  depending on flow parameters, as seen in Table 11. [5,6]

#### Table 11: Physical properties of water coolant. [5]

| Coolant | Tinlet °C | ΔT °C | Pressure (bar) | ΔPcore (bar) | vz (cm/s) | Density (g/cc) | hs (W/cm2K) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| H2O | 300 | 20 | 100 | 2 | 400 | 0.7 | 2.8-4.5 |

For the currently proposed films, roughness values (Ra) of around 10μin (0.25 microns) for the 5 and 10-micron thick films have been deposited in experiments. [14] This value is used with two perturbations of 50% decrease (5μin) and a 50% increase (15μin) in roughness to illustrate the change on the heat transfer coefficient. We assume a typical flow velocity of 4.0 m/s and a bulk temperature of 315°C (used for fluid parameters). [6] From the heat transfer coefficient equation derived in the Methodology section coupled with the Moody diagram, the change in the heat transfer coefficient due to the film’s roughness is obtained.

#### Table 12: Impact on heat transfer coefficient with various film friction factors.

| Film Roughness μin | Darcy Friction Factor ƒ | Nusselt Number | Heat Transfer Coefficient Wcm2K |
| --- | --- | --- | --- |
| 5 (0.127μm) | 0.014 | 528.26 | 2.97 |
| 10 (0.254μm) | 0.015 | 566.66 | 3.18 |
| 15 (0.381μm) | 0.016 | 605.13 | 3.40 |

The film’s roughness shows a significant (about 10 %) change in the heat transfer coefficient between the film and the coolant. Although, the calculated heat transfer coefficient values all remain in the range of the typical Zr-coolant under normal operations, where under normal flow parameters Zr-clad has a friction factor of around 0.014. [5]

To further investigate the effect the roughness produces on the system, the pressure drop across the flow channel is evaluated. Using the same film roughness value and the perturbations (i.e. 5 and 15μin), the new pressure drop is acquired using the ΔP equation in the Methodology section. The results from this study are illustrated in Table 13.

#### Table 13: Pressure drop induced by film roughness along the flow channel.

| Film Roughness μin | Friction Factor ( ƒ ) | Pressure Drop (psi) |
| --- | --- | --- |
| 5 (0.127μm) | 0.014 | 1.67 |
| 10 (0.254μm) | 0.015 | 1.79 |
| 15 (0.381μm) | 0.016 | 1.91 |

The small roughness values introduce a minor pressure drop along channel, all of which are below 2.0 psi. For comparison, Duderstadt gives typical pressure drop for a PWR due to friction as 0.40 bar (5.8 psi) in the core (not the full loop). This value is over double the pressure loss due to film friction. [5] The pressure drop due to channel friction is used to calculate the pumping power required to pump the coolant through the primary loop Ppump=ΔPtotal Acs vz. If the frictional pressure drop along the channel remains smaller than the Zr-clad frictional loss, the required pumping power will decrease which can be advantageous due to the decrease in power consumption for the primary coolant pumps.

## 3.5:  Parameter Uncertainty Analysis

To reiterate, the implementation of the ABH method for an estimate of the thermal utilization and the centerline temperature of the fuel pin are reassessed using uncertainty probability for certain parameters. For each of the respective equations, the variables which uncertainty occurs are as follows with the corresponding percent perturbation used:

ABH Method: PFO (10%) and  ΣabsM (20%)

Centerline Temperature: hs (15%) and kfilm (20%)

To illustrate the impact the film impacts on the multiplication factor coupled with parameter uncertainties, the keff is obtained by using normal values for the other parameters in the four-factor formula (e.g. fast fission factor, reproduction factor, and resonance escape probability). [5] The standard deviations for the ABH and the centerline temperature for each film are shown in Table 14.

#### Table 14: Uncertainty obtained for ABH method and centerline temperature.

|  | Film Thickness (microns) | σkeff | σTemp °C |
| --- | --- | --- | --- |
| Reference | - | 0.0113 (0.74%) | 8.913 (0.49%) |
| ZrO2 | 5 | 0.0108 (0.71%) | 8.935 (0.48%) |
| TiAlN | 5 | 0.0102 (0.67%) | 8.923 (0.48%) |
| Ti2AlC | 5 | 0.0113 (0.74%) | 8.921 (0.48%) |
| Ti3AlC2 | 5 | 0.0110 (0.72%) | 8.920 (0.48%) |
| ZrO2 | 10 | 0.0109 (0.72%) | 8.924 (0.48%) |
| TiAlN | 10 | 0.0110 (0.73%) | 8.925 (0.48%) |
| Ti2AlC | 10 | 0.0111 (0.73%) | 8.930 (0.49%) |
| Ti3AlC2 | 10 | 0.0113 (0.75%) | 8.939 (0.49%) |

These uncertainty (standard deviation) values are applied to the previously calculated values to illustrate the range of uncertainty within the calculation, as seen in Table 15. The multiplication factor used was obtained from the MCNP KCODE calculation, where, as all other parameters are not greatly impacted by the additional film region, will yield the uncertainty.

#### Table 15: Multiplication factor and centerline temperature with uncertainty.

|  | Film Thickness (microns) | keff | TCL °C |
| --- | --- | --- | --- |
| Reference | - | 1.5204 ± 0.0113 | 1834.80 ± 8.913 |
| ZrO2 | 5 | 1.4896 ± 0.0108 | 1840.89 ± 8.935 |
| TiAlN | 5 | 1.4876 ± 0.0102 | 1837.22 ± 8.923 |
| Ti2AlC | 5 | 1.4887 ± 0.0113 | 1835.18 ± 8.921 |
| Ti3AlC2 | 5 | 1.4894 ± 0.0110 | 1835.07 ± 8.920 |
| ZrO2 | 10 | 1.4893 ± 0.0109 | 1847.01 ± 8.924 |
| TiAlN | 10 | 1.4874 ± 0.0110 | 1839.66 ± 8.925 |
| Ti2AlC | 10 | 1.4865 ± 0.0111 | 1835.66 ± 8.930 |
| Ti3AlC2 | 10 | 1.4871 ± 0.0113 | 1835.38 ± 8.939 |

The largest uncertainty in the multiplication factor 0.0113 is less than one percent of the calculated keff value. This is also true for the centerline temperature, where the maximum uncertainty 8.939°C is well below one percent of the centerline temperature. For the parameters selected for the uncertainty analysis coupled with the relative percent perturbations applied to each variable, the uncertainty remains minimal in both calculations.

## 3.6:  Temperature Change during Flow Transient

To understand the impact each film introduces during the transient, each simulation will be evaluated against a reference, no-film fuel pin. The analysis is carried out using MATLAB. First, the flow velocity is varied slower than the power density, causing a momentary mismatch in fluid temperature. That is, using the previous equations from the Methodology section which expressed the time-dependent forms of the linear power density and coolant flow velocity, we can define the equations in terms of their respective time constants (i.e. 25 seconds for the linear power density, 60 seconds for the flow velocity).

q't=12q'0exp-λ1t+1=12q'0expln0.525t+1                     (Eq.53)

vt=12v0exp-λ2t+1=12v0expln0.560t+1                     (Eq.54)

As the two parameters approach a steady-state value, the change in moderator temperature in the channel rises to the original value (i.e. 20°C in our case). A linear power density value of 160 W/cm and a flow velocity of 4.0 m/s are used for initial values, respectively. Figure 10 illustrates a normal fuel pin simulation.

### Figure 10: No-film region simulation illustrating the two varying parameters and the impact on the moderator temperature change along the channel.

From the figure, the top right plot illustrates the difference between the inlet and outlet temperature of the coolant. The transient introduces the momentary mismatch between the flow and power density, decreasing the temperature difference across the channel until both the flow and power approach a steady-state value. This simulation illustrates how the films impact the coolant’s temperature difference along the channel. Additionally, the heat transfer coefficient will be decreased to adequately show the how the film’s roughness can change a transient (i.e. h changed from 3.4Wcm2K to 3.0Wcm2K only on the film simulations).

Using the same time values to vary the flow velocity and power density, we can obtain a model for each of the films. Figures 11 through 14 illustrate each film’s simulation output using a 10μm film thickness.

### Figure 11: Power transient followed by slower velocity change using 10μm ZrO2 film.

### Figure 12: Power transient followed by slower velocity change using 10μm TiAlN film.

### Figure 13: Power transient followed by slower velocity change using 10μm Ti2AlC film.

### Figure 14: Power transient followed by slower velocity change using 10μm Ti3AlC2 film.

As a second simulation, the time constants are switched so that the flow velocity decreases sharper than the power density resulting in a momentary increase in moderator temperature across the channel (i.e. longer time change for the linear power density). Figure 15 shows the reference simulation.

### Figure 15: Reference run for flow velocity variation followed by power density.

Due to the slower power change, the outlet temperature of the coolant increases momentarily until the power and the flow both approach a steady-state value, as seen in the top right of Figure 15. That plot should be used to compare each film’s impact on the peak temperature and time elapsed to become steady (i.e. validate the film has little effect on the transient). Figures 16 through 19 show each film’s transient for this simulation.

### Figure 16: Flow velocity transient followed by slower power density change using 10μm ZrO2 film and lower heat transfer coefficient.

0

### Figure 17: Flow velocity transient followed by slower power density change using 10μm TiAlN film and lower heat transfer coefficient.

### Figure 18: Flow velocity transient followed by slower power density change using 10μm Ti2AlC film and lower heat transfer coefficient.

### Figure 19: Flow velocity transient followed by slower power density change using 10μm Ti3AlC2 film and lower heat transfer coefficient.

In all film simulations, the change in moderator temperature along the channel approaches a steady state nearly identical to that of the normal fuel rod. Even using the higher thermal conductivity films (e.g. Ti2AlC, Ti3AlC2) and the decrease in the heat transfer coefficient show little difference due to the small film thickness.

# 4:  Conclusion

The assessments within this report evaluate four ceramic coatings to determine their  impact on fuel performance during operation. With film thicknesses of 5 and 10 microns, the reactivity change is less than 0.5% from the reference and the corresponding increase of fuel cycle length is less than 3 days and burnup values around 48.5 MWd/kg for all cases. The maximum temperature of the fuel assessed with the film region present is well below the melting point of the fuel (maximum of 1847°C) yielding 0.67% variation from the reference, even with high power density values of 460 W/cm. The roughness introduced by the film to the coolant flow channel results in small changes in heat transfer (about 10 %) and pressure change along the channel, both of which are within the Zr-alloy cladding values. During a flow and power transient, the coolant’s temperature changes along the channel are about the same for all films and thicknesses relative to a reference case with no-film. The results show that thin (5 to 10 microns) ceramic films applied to the moderator/coolant side of the Zr-clad in a LWR produce small (generally less than 2%) variations in reactor performance parameters relative to those for reference conditions.

# 5:  Future Work

In this study, material parameters were not temperature dependent; thus, further analysis is required for temperature-dependent scenarios (e.g. maximum temperature calculations).  As more refined values of the film’s properties become available, the calculations implemented here should be repeated. Transient analyses are also important to evaluate the film’s effectiveness during normal and accident conditions (e.g. power ramps, LOCA, high temperature scenarios, etc.). Currently, the transient reactor test facility (TREAT) at Idaho National Laboratory (INL) is used to test new fuel concepts under reactor transient conditions. [15] This analysis is essential to verify the film’s effectiveness during various scenarios.

# Works Cited

- Nuclear Energy Research and Development Roadmap - Report to Congress. United States Department of Energy. Office of Nuclear Energy. April 2010.

- Bragg-Sitton, Shannon. “Development of advanced accident tolerant fuels for commercial LWR.” Nuclear News. Pages 83-91. March 2014.

- Bragg-Sitton, Shannon. Advanced LWR Nuclear Fuel Cladding System Development: Technical Program Plan. DOE Office of Nuclear Energy. December 2012. Report No. INL/MIS-12-25696.

- Ceramic Coatings for Clad (The C3 Project): Advanced Accident-Tolerant Ceramic Coatings for Zr-Alloy Cladding. CFP Proposal IRP 12-4722. DOE. NEUP-IRP.

- Duderstadt, James J. and Louis Hamilton. Nuclear Reactor Analysis. 1976. John Wiley & Sons, Inc.

- Todeas, Neil E. and Kasimi, Mujid S. Nuclear Systems: Thermal Hydraulic Fundamentals. Volume 1. 2nd Ed. CRC Press. 2012.

- MCNP — A General Monte Carlo N-Particle Transport Code, Version 5. Los Alamos National Laboratory. LA-UR-03-1987 / LA-CP-03-0245. Volume I&II. 2003.

- Driscoll, M.J. Thomas Joseph Downar, and E. E. Pilat. The Linear Reactivity Model for Nuclear Fuel Management. American Nuclear Society. January 1, 1990.

- Schmidt, Henderson, and Wolgemuth. Introduction to Thermal Sciences. John Wiley & Sons. 2nd ed. 1993.

- @Risk Analysis Software using Monte Carlo Simulations for Excel. Palisade Corporation. Ithaca, NY. 2014. <https://www.palisade.com/risk/>.

- Rasmussen, Inge. Optical Monitoring and X-ray Absorption Spectroscopy for Studies of Wear on Thin Films. December 2010. <http://www.nbi.ku.dk/english/research/phd_theses/phd_theses_2011/inge_l_rasmussen/inge_l_rasmussen.pdf>.

- Zirconia: Ceramic Properties Tables. Ferro Ceramic Grinding, Inc. Willmington, MA. <http://www.ferroceramic.com/zirconia.htm>.

- About ZrO2. K-Style Advanced Ceramics. P.R. China. 2006. <http://www.zro2.com/Top-About-ZrO2.htm>.

- "Cross Section Metallography of TiAlN Coated ZIRLO." Ceramic Coating of Cladding Meeting. Pennsylvania State University. 12 July 2013. Lecture.

- Ehresman, Teri. “Transient Reactor Test Facility.” US DOE. Idaho National Laboratory. Web. Jan. 2015. <http://www.inl.gov/research/transient-reactor-test-facility>.

# Appendix

Various calculations and techniques were also undertaken during the study, some of which was insignificant or deemed unnecessary after finishing the analysis. Following this is the evaluation of film depletion and new high absorbing film compounds.

##### Film Depletion Approximation

Depletion of the ceramic films during operation is important in understanding how the film will respond over the lifetime of the fuel. In order to estimate the depletion of an isotope, there are two standard approximations, constant power and constant flux.  These approximations for isotropic depletion are quite different, as illustrated in Figure 20 below. [5]

### Figure 20: Depletion of a single isotope comparison using constant flux and constant power approximations.

Constant Flux Approximation

Assuming that over the lifetime of the fuel the flux is treated as constant, the number density of an isotope can be approximated. That is, the burnup or depletion of an isotope can be expressed by the simple rate equation: [5]

dNdt=-Nr,t σabs ϕr,t			   	(Eq.55)

Thus by assuming a constant flux over the lifetime of the fuel:

ϕr,t=ϕ0 						   (Eq.56)
Nt=N0e-σabs ϕ0 t    				   (Eq.57)

Constant Power Approximation

By assuming a constant reactor power, the depletion of the number density of an isotope can be obtained. This implies:

dNdt=-σabs N ϕ=P0wa 				    (Eq.58)

Where, wa is the energy released per neutron absorption ( wa= σfσa wf ).

By integrating this equation, one finds:

Nr,t=Nr,0-P0rwat 				     (Eq.59)

This equation differs greatly from that of the constant flux approximation. However, over short time intervals, the solutions of both approximations are similar, since the previous constant power equation becomes: [5]

Nr,t≅Nr,01-σabsϕ0t			       (Eq.60)

Using a constant flux value of  1013ncm-s , the isotropic depletion of the three ceramic films were calculated via MATLAB using both approximations. Table 16 lists the isotope depletion using the constant power approximation and Table 17 lists the depletion using the constant power approximation. Both calculations use a fuel cycle length of 1000 days.

#### Table 16: Depletion of each film isotope using constant power approximation equation.

| Film | Isotope | Flux Approximation (n /cm-s) | Isotope Depletion (%) |
| --- | --- | --- | --- |
| ZrO2 | Zr | 1013 | 0.08% |
|  | O | 1013 | 8.65E-5% |
| TiAlN | Ti | 1013 | 2.51% |
|  | Al | 1013 | 0.10% |
|  | N | 1013 | 0.81% |
| Ti3AlC2 | Ti | 1013 | 2.51% |
|  | Al | 1013 | 0.10% |
|  | C | 1013 | 0.002% |

#### Table 17: Isotropic Depletion using constant flux approximation equation.

| Film | Isotope | Flux Approximation (n /cm-s) | Isotope Depletion (%) |
| --- | --- | --- | --- |
| ZrO2 | Zr | 1013 | 0.07% |
|  | O | 1013 | 8.63E-5% |
| TiAlN | Ti | 1013 | 2.48% |
|  | Al | 1013 | 0.10% |
|  | N | 1013 | 0.80% |
| Ti3AlC2 | Ti | 1013 | 2.48% |
|  | Al | 1013 | 0.10% |
|  | C | 1013 | 0.001% |

##### High Absorption Films

Preliminary evaluation of new film compounds was also conducted. A heavy absorber material is proposed to be added to the film, which could be beneficial to the system. Such isotopes with high absorption cross sections that are within a nuclear reactor are boron, gadolinium, indium, and xenon. To assess the impact an isotope with a high absorption cross-section yields on the system, two films are utilized: B4C and BN.

MCNP and the ABH method are both used to evaluate the change in the multiplication factor (k). Both films are assessed at 10 micron and 100 micron thicknesses. In order to lessen the initial affect the high absorption cross section of the 10B isotope (σa≅3850 b), a ratio of 10B to 11B is used (natural boron is roughly 80% 11B and 20% 10B). Three ratios are used:

- 20% 10B, 80% 11B

- 1% 10B, 99% 11B

- 0.1% 10B, 99.9% 11B

The cross-section library used for this analysis is for n,γ reactions. Tables 18 and 19 list the change keff using MCNP and the ABH method for 10 micron and 100 micron thicknesses.

#### Table 18: Multiplication factor with varying boron concentration ratios at 10-micron film.

| Film | Thickness | B-10 / B-11 Concentration | keff (MCNP) | Difference (MCNP) | Difference (ABH) |
| --- | --- | --- | --- | --- | --- |
| Reference | - | - | 1.520 | - | - |
| B4C | 10 | 20% / 80% | 1.016 | 33.14% | 25.84% |
| B4C | 10 | 1% / 99% | 1.477 | 2.84% | 1.64% |
| B4C | 10 | 0.1% / 99.9% | 1.516 | 0.29% | 0.10% |
| BN | 10 | 20% / 80% | 1.127 | 25.84% | 48.30% |
| BN | 10 | 1% / 99% | 1.488 | 2.10% | 4.60% |
| BN | 10 | 0.1% / 99.9% | 1.515 | 0.35% | 0.62% |

#### Table 19: Multiplication factor for different boron concentration ratios at 100-micron film.

| Film | Thickness | B-10 / B-11 Concentration | keff (MCNP) | Difference (%) | Difference (ABH) |
| --- | --- | --- | --- | --- | --- |
| Reference | - | - | 1.520 | - | - |
| B4C | 100 | 20% / 80% | 0.389 | 74.38% | 77.30% |
| B4C | 100 | 1% / 99% | 1.192 | 21.56% | 14.02% |
| B4C | 100 | 0.1% / 99.9% | 1.489 | 2.05% | 0.94% |
| BN | 100 | 20% / 80% | 0.464 | 69.49% | 88.38% |
| BN | 100 | 1% / 99% | 1.265 | 16.79% | 28.11% |
| BN | 100 | 0.1% / 99.9% | 1.469 | 3.38% | 4.69% |

From Table 18 and 19 it should be noted the impact 10B produces to the multiplication factor. The films would most likely be destroyed, thus changing the atomic compound of the film. The impact on fuel cycle is not shown here and is more difficult to understand than the other four films considering the boron deplete fairly rapids and burn out at the beginning of the fuel life cycle.  This quick depletion could be useful when attempting to compensate for excess reactivity during early stages of core life.

## PWR Data

The information on parameters for the PWR analysis used the values from in Nuclear Reactor Analysis by Duderstadt and Hamilton. [5]

#### Table 20: Reactor Information from Duderstadt text Appendix H. [5]

| General Data | PWR (Westinghouse) |
| --- | --- |
| Thermal Output (MWth) | 3411 |
| Electrical Output (MWe) | 1150 |
| Efficiency (%) | 33.7 |
| Fuel Type | UO2 |
| Coolant | H2O |
| Structural Material | Zircaloy |
| Moderator | H2O |
| Core Data |  |
| Active Height (cm) | 366 |
| Equivalent Active Diameter (cm) | 337 |
| Height / Diameter | 1.09 |
| Active Core Volume (L) | 32,800 |
| Average Core Power Density (kW/L) | 104 |
| Fuel Weight (kg) | 90,200 |
| Specific Power (kW/kgU) | 37.8 |
| Burnup (MWd/MTU) | 33,000 |
| C.R. | 0.5 |
| Fuel Type Assembly | Square Bundles |
| Number of Assemblies | 193 |
| Fuel-element array | 17 x 17 |
| Assembly Dimension (cm) | 21.4 x 21.4 |
| Assembly Pitch (cm) | 21.5 |
| Number of Fuel Elements / Assembly | 264 |
| Total Number of Fuel Locations | 50,952 |
| Fuel Element Date Type | Clad rod |
| Fuel-element Pitch (cm) | 1.25 |
| Fuel Element O.D. (cm) | 0.94 |
| Pitch / Diameter | 1.32 |
| Clad Thickness (cm) | 0.0572 |
| Fuel-pellet diameter (cm) | 0.819 |
| Pellet-Clad Gap (cm) | 0.0082 |
| Fuel Enrichment | 2.1/2.6/3.1 |
| Thermal Hydraulic Data |  |
| System Pressure (bar) | 155 |
| Coolant Flow (106 kg/hr) | 62 |
| Average Linear Power Density (W/cm) | 178 |
| Maximum Linear Power Density (W/cm) | 426 |
| Average Heat Flux (W/cm2) | 68.5 |
| Maximum Heat Flux (W/cm2) | 183 |
| Minimum DNBR | 1.3 |
| Inlet Temperature (C) | 300 |
| Outlet Temperature (C) | 332 |
| Maximum Fuel Temperature | 1788 |

## Code Implementation

Example MCNP multiplication factor calculation (KCODE) for Ti2AlC film at 10micron thickness. Single fuel pin, infinite in length, with 5 regions present: fuel, gap, clad, film, and moderator. The enrichment used is 5% U-235 with 95% U-238. The keff calculation implemented 1000 histories per cycle, an initial guess of 1.0, with 1000 cycles total, while skipping the first 50. It should be noted that the format shown here may be different due to formatting issues within the report, but the syntax is correct.

MCNP Analysis of Ti2AlC Ceramic Film

C ---------------

C Cell

C ---------------

1 1 -10.96 -1 imp:n=1	$ fuel

2 0	1 -2 imp:n=1 		$ gap

3 2 -6.49 2 -3 imp:n=1	$ clad

4 3 -4.1 3 -4 imp:n=1	$ Ti2AlC film

5 4 -0.9982 4 -5 imp:n=1 	$ moderator

0 0         5 imp:n=0	$ end void

C ---------------

C Surface

C ---------------

1 CY 0.4095

2 CY 0.4177

3 CY 0.4749

4 CY 0.4759		$ 10 micron thickness

+5 CY 0.70524 $+ indicates white boundary

C ---------------

C Data

C ---------------

mode n

M1   8016  2.0       $ UO2 Fuel

92235  0.05

92238	0.95

M2 40090 1.0		$ Zr Clad

M3 22048 2.0 13027 1.0 6012 1.0 $ Ti2AlC Film

M4 1001 2.0 8016 1.0	$ H2O Mod

kcode 1000 1.0 50 1000 $ Keff: 1000histories/cycle, 1 K_guess, first 50 cycles of 1000 skipped

ksrc 0 0 0		$ Keff Source location (x,y,z)

print

The ABH method used to expand the thermal utilization factor within the four-factor formula is shown here. The code is written within MATLAB software, with each film having its own code (ran into syntax errors when compiled all four films into one). Here is an example for Ti2AlC film at a 5 micron thickness. Again, readers are warned that due to formatting in report, certain line-movement, syntax, etc., the code may present certain errors due to this formatting.

%% Inputs/Assumptions, Westinghouse PWR Parameters / Appendix H Duderstadt

Dpin = 0.819;       %Fuel Pin Diameter (cm)

Pitch = 1.25;       % (cm)

a = Dpin/2;         %Fuel radius (cm)

b = Pitch/(pi^0.5); %Moderator-Cell Radius (cm)

ACell = Pitch^2;    %Area of cell (cm^2)

rFuel = Dpin/2;     % cm (radius of the fuel element)

tGap = 0.0082;      % cm (thickness of the air gap)

tClad = 0.0572;     % cm (thickness of the cladding)

% Volume Fractions

Vf = (rFuel^2*pi)/(Pitch^2); %Fuel Volume (assume 1cm length) (cm^3)

Vgap = ((pi*(rFuel+tGap)^2)-Vf)/(Pitch^2);

Vclad = (pi*((rFuel+tGap+tClad)^2)-(Vf+Vgap))/(Pitch^2);

tFilm = 0.0005; %Film Thickness (cm)

VFilm = ((pi*(rFuel+tGap+tClad+tFilm)^2)-(pi*(rFuel+tGap+tClad)^2))/(Pitch^2);

Vm = (ACell-(pi*(tGap+tClad+rFuel+tFilm)^2))/(Pitch^2);

Vm1 = (ACell - (pi*(tGap+tClad+rFuel)^2))/ACell; % Mod Vol w/out film

coatings = {'Ti2AlC'};

% Film Data %

Nav = 6.02*(10^23); %Avogadro's Number (Atom/Mole)

dTi2AlC = 4.0; %Density Ti2AlC Film (g/cc)

WTi2AlC = 134.726; %Atomic Weight Ti2AlC (g/mole)

NTi2AlC = (Nav*dTi2AlC)/WTi2AlC; %No. Density Ti2AlC (1/cc)

SigmaTi2AlC = 11.8*10^-24; %Abs. MicroCS (b to cm^-2)

%Macroscropic Cross-section for Ceramic Films:

SigmaFilm = SigmaTi2AlC*NTi2AlC;

% Macroscopic Cross-sections from Appendix H in Duderstadt %

SigmaMa = 0.022;    %Abs. MacroCS Moderator (cm^-1)

SigmaFa = 0.169;    %Abs. MacroCS Fuel (cm^-1)

SigmaFs = 0.372;    %Scatter MacroCS Fuel (cm^-1)

SigmaFt = SigmaFa+SigmaFs; %Total MacroCS Fuel (cm^-1)

SigmaMt = 3.45;     %Total MacroCS H2O (cm^-1)

SigmaMs = 3.45;     %Scatter MacroCS H2O (cm^-1)

SigmaMa1 = (Vm/(Vm+VFilm)*SigmaMa)+(SigmaFilm*VFilm/(Vm+VFilm)); %Volume Avg. MacroCS

u_o = 1-0.676;      %App.A for H2O

lMtr = (SigmaMt-(u_o*SigmaMs))^-1; %Eq.4-150 Duderstadt, m.f.p. Moderator

Diff_length = 0.7104*lMtr;

Lm = (Diff_length/SigmaMa)^0.5; %Used in Lattice Function

S_f = pi*Dpin; %Surface Area of Fuel region (pi*D)*1cm

% Fig.10-11 Duderstadt for ABH method %

abh = a*SigmaFt;

alpha = -0.0064*abh^2 + 0.0679*abh + 0.0022; %Best fit f(x)-

beta = -0.0038*abh^2 + 0.0162*abh + 0.0122;  %-for Fig.10-11

% Fig.10-13 Duderstaft for extrapolation dist. (d)

RMtr = Pitch/pi^0.5/lMtr;

d = 0.7104*lMtr;

% Bessel Functions for Lattice Fuction %

I0a = besseli(0,a/Lm);

K0a = besselk(0,a/Lm);

K1a = besselk(1,a/Lm);

I1a = besseli(1,a/Lm);

I1b = besseli(1,b/Lm);

K1b = besselk(1,b/Lm);

% Bessel Functions for Lattice Function with Film Cross-Section added %

lMtrf = ((SigmaMa1+SigmaMt)-(u_o*SigmaMs))^-1; %Eq.4-150 Duderstadt, m.f.p. Moderator

d_film = 0.7104*lMtrf;

Lmf = (d_film/SigmaMa1)^0.5;

I0af = besseli(0,a/Lmf);

K0af = besselk(0,a/Lmf);

K1af = besselk(1,a/Lmf);

I1af = besseli(1,a/Lmf);

I1bf = besseli(1,b/Lmf);

K1bf = besselk(1,b/Lmf);

%% Calculations

Pfo = S_f/(4*Vf*SigmaFa); %First-Flight Escape Prob. Approx. Eq.10-49 Duderstadt

%Reference Run

Lattice = ((b^2-a^2)/(2*a*Lm))*((I0a*K1b+K0a*I1b)/(I1b*K1a-K1b*I1a)); %Lattice Function

fREF = (((SigmaMa*Vm1)/(SigmaFa*Vf))*(1+(SigmaFa/SigmaFt)*((1-Pfo)/Pfo-a*SigmaFt)*(1+alpha*(SigmaFs/SigmaFt)...

+ beta*(SigmaFs/SigmaFt)^2))+((a*d/(2*Lm^2))-a*SigmaMa)*(Vm1/Vf)+Lattice)^-1; %Reference Thermal Utilization

fprintf(1,'The thermal utilization for the reference run without the film region is %0.4f.\n',fREF);

%Film Runs

LatticeFilm =((b^2-a^2)/(2*a*Lmf))*((I0af*K1bf+K0af*I1bf)/(I1bf*K1af-K1bf*I1af));

fFILM = (((SigmaMa1*Vm)/(SigmaFa*Vf))*(1+(SigmaFa/SigmaFt)*((1-Pfo)/Pfo-a*SigmaFt)*(1+alpha*(SigmaFs/SigmaFt)...

+ beta*(SigmaFs/SigmaFt)^2))+((a*d/(2*Lmf^2))-a*SigmaMa1)*(Vm/Vf)+Lattice)^-1;

Difference = abs((fFILM-fREF)/fREF*100);

s = coatings{1};

fprintf(1,'The thermal utilization for the %5s film run is %0.4f.\nThe percent change from the reference is %2.3f percent for a %0.0f-micron film thickness.\n',...

s,fFILM,Difference,tFilm*1E4);

Presented below is the one-dimensional thermal analysis using the circuit analogy. The code is written and implemented using MATLAB. All four films and thicknesses (i.e. 5 and 10 microns) are implemented in the code. The percentages calculated are found via the reference run also within the code.

clear all; clc;

%% Thermal Analysis of the effects Coatings

rFuel = 0.4095;     % cm (radius of the fuel element)

tGap = 0.0082;      % cm (thickness of the air gap)

tClad = 0.0572;     % cm (thickness of the cladding)

qPrime = 460;       % W/cm (Linear Power Density, pg. 419 Nuc Sys)

kFuel = 0.025;      % W/cm K (thermal conducitivity of fuel)

Rg = rFuel + tGap/2;% cm (Average radius of air gap)

hg = 0.75;          % W/cm^2 K (heat transfer coefficient gap, pg. 419 Nuc Sys)

kClad = 0.1070;     % W/cm K (thermal conducitity of the clad)

Rci = rFuel + tGap; % cm, (inner cladding radius)

Rco = Rci + tClad;  % cm (outer cladding radius)

h = 3.3;            % W/cm^2 K (heat transfer coefficient of water to film)

%% Reference Fuel Case

% The reference fuel pin does not have the coating

Roo = Rco;

deltaTRef = qPrime/(2*pi)*(1/(2*kFuel)+ 1/(Rg*hg) + log(Rco/Rci)/kClad + 1/Roo/h);

deltaTRefClad = qPrime/(2*pi)*(log(Rco/Rci)/kClad + 1/Roo/h);

fprintf(1,'The change in temperature across a reference fuel pin: %5.2f K\n',deltaTRef);

fprintf(1,'The change in the inner cladding radius: %5.2f K\n',deltaTRefClad);

%% Different Coatings

coatings = {'ZrO_2','TiAlN','Ti_2AlC','Ti_3AlC_2'};

k = [2, 5, 30, 40]/1000;   % W/cm k (thermal conducivity of film coating)

sigma = [0.01, 0.001]; % cm (thickness of coating)

deltaTFuel =  @(ko,sigmao) qPrime/(2*pi)*(1/(2*kFuel)+ 1/(Rg*hg) + log(Rco/Rci)/kClad + 1/(2*pi*(Rco+sigmao)*ko/sigmao)+1/Roo/h);

deltaTClad =  @(ko,sigmao) qPrime/(2*pi)*(log(Rco/Rci)/kClad + 1/(2*pi*(Rco+sigmao)*ko/sigmao)+1/Roo/h);

precentChange = @(T) (T-deltaTRef)/deltaTRef*100;

for j = 1:numel(sigma)

fprintf(1,'%3.0f um Coating \t\t   Fuel Pin\t Cladding Outer\t  Reference \t Precent Change\n',sigma(j)*1E4);

fprintf(1,'\t\t\tk_film  \tTemperature \tDelta T\n');

for i=1:numel(coatings)

dT = deltaTFuel(k(i),sigma(j));

dTClad = deltaTClad(k(i),sigma(j));

s = coatings{i};

fprintf(1,'%10s (%3.0f W/cm-K) \t %5.2f \t %5.f \t\t %6.2f \t %5.4f \n',...

s,k(i)*1000,dT,dTClad,dT-deltaTRef,precentChange(dT));

end

end

Roughness impact on the heat transfer coefficient and pressure drop along the flow channel is shown below. The code is written in MATLAB and shows three friction factors (see Moody diagram) of 0.014, 0.015, and 0.016.

% Evaluation of Relative Roughness Impact on heat transfer coef.

clear all; close all; clc;

%% Problem Calculations

film_thickness = 0.01; %cm (100micron)

fuel_diameter = 0.95; %cm

d_hydraulic = (fuel_diameter+2*film_thickness);

flow_velocity = 400; %cm/s

% Moderator Values (H20 at 300C, Intro. Thermal Sciences by Schmidt)

mu = 0.0858*10^-3; %kg/m-s Viscosity

cp = 5.78; %J/g-C Specific Heat

k = 0.545; %W/m-C Thermal Conductivity

% Heat Transfer values and roughness

friction = [0.014,0.015,0.016]; %See Moody Chart

Re = (flow_velocity*d_hydraulic)/(100*100*0.1205*10^-6)

Pr = (cp*mu*1000)/k; %Prandtl #

for i=1:length(friction)

Nu(i) = ((friction(i)/8)*(Re-1000)*Pr)/(1+12.7*sqrt(friction(i)/8)*(Pr^(2/3)-1)); %Nusselt #

h(i) = (k/100*Nu(i))/d_hydraulic;

delta_P = 1000*9.81*(friction(i)*(400/d_hydraulic)*(flow_velocity/100/(2*9.81)))/1000;

fprintf('Heat transfer coefficient (h) for %.3f (Darcy) friction factor:%5.2f W/cm2-K\n',friction(i),h(i));

fprintf('\tPressure drop: %.2f kPa (%.2f psi)\n',delta_P,delta_P*0.145037738);

end

Transient analysis for varying time-dependent flow velocity and power density is shown below. MATLAB is used for the analysis. In this example, the power density is varied faster (25seconds) than the flow velocity (60seconds), creating a momentary decrease in coolant temperature change along the channel. All films are implemented with the code at a thickness of 10 microns.

% Approx. Fuel CL Temp. with exponential change in q' & mass flow

% For each film, only the thermal conductivity will change and thickness.

% Multiple flows are given to understand the placement (up the rod) and

%   the change in the centerline temperature.

% The electrical resistor analogy is used for linear heat transfer

%   across the fuel pin.

clear all; clc; close all; format compact;

%% FILM Properties %%

sigma = 0.001;      %Coating Thickness (cm)

films = {'ZrO2','TiAlN','Ti2AlC','Ti3AlC2'};

kFilm = [2,5,30,40]/1000;     %W/cm-K (thermal cond. of film)

%% Fuel/Flow Properties %%

Tin = 295+273;      %K (Initial Temp.)

rFuel = 0.4095;     %cm (Radius of the fuel element)

H = 12*12*2.54;     %cm (Assuming 12ft fuel assembly length)

A = 0.824;          %cm^2 (Cross-sectional flow area)

v0 = 4*100;         %cm/s (H20 flow rate)

rho = 0.001;        %kg/cc (H2O density, Table K.2 in Todreas p.975)

m0 = rho*A*v0;      %kg/s (H2O mass flow)

cp = 5.742E3;       %J/kg-K (Coolant Specific heat, Todreas p.975)

% Initial Power based on 5-m/s flow

q0 = (rho*A*500*cp*(25)/H);

%

kFuel = 0.025;      %W/cm-K (U-fuel thermal cond.)

tGap = 0.0082;      %cm (Gap Thickness)

Rg = rFuel + tGap/2;%cm (Average radius of air gap)

hg = 0.75;          %W/cm^2 K (heat transfer coefficient gap, pg. 419 Nuc Sys)

tClad = 0.0572;     %cm (thickness of Zr-cladding)

kClad = 0.1070;     %W/cm K (thermal conductivity of the fuel)

Rci = rFuel + tGap; %cm (inner cladding radius)

Rco = Rci + tClad;  %cm (outer cladding radius)

hs = 3.4;           %W/cm^2-K (heat transfer coefficient of water to clad)

Roo = Rco + sigma;  %cm (radius to outside film)

visc_k = 0.13E-2;   %cm^2/s (kinematic viscosity at 300-C)

Re=(v0*2*Roo)/visc_k; %Unitless (Reynolds No. used with Moody Chart)

%% Calculations %%

z=0; %Starting position

for k=1:length(films) %Stepping through films

for t=1:600 %Time steps in Seconds (due to eigenvalues-lambdas in sec^-1)

%qPrime(t) = (dTfluid*m0*cp*(exp(log(0.25)/60*t)+1))/(exp(log(0.25)/100*t)+1); %Fixed

qPrime(t) = (0.5*q0*(exp(log(0.5)/25*t)+1)); %Linear Power change to 0.5q0

v(t) = 0.5*v0*(exp(log(0.5)/60*t)+1); %Flow velocity change to 0.5m0

m(t) = rho*A*v(t); %kg/s (H2O mass flow)

for i=1:145

Tr1(i) = Tin-((qPrime(t)*H/m(t)/cp/pi)*(cos(pi*z/H)-1));

T1(i) = qPrime(t)*sin(pi*z/H)/(2*pi)*(1/(2*kFuel)+1/(Rg*hg)+log(Rco/Rci)/kClad+1/(2*pi*(Rco+sigma)*kFilm(k)/sigma)+1/Roo/hs);

T_CL(i) = Tr1(i) + T1(i);

z=z+2.54;

end

z=0; %Resets position for next time interval

Delta_TFluid(t)=Tr1(145)-Tr1(1); %Change in mod temp for each time step

Max_CL_Film(t)=max(T_CL); %Assigning T_CL Max for each time step

end

%% Plots

figure(k)

subplot(2,2,1)

plot(Max_CL_Film,'Linewidth',2)

title('Max C.L. Fuel Temp','FontWeight','bold')

xlabel('Time (seconds)');

ylabel('Temperature (C)');

grid on

subplot(2,2,2)

plot(Delta_TFluid,'-r','Linewidth',2)

title('Fluid Temperature through channel','FontWeight','bold')

xlabel('Time (seconds)');

ylabel('Temperature (C)');

grid on

subplot(2,2,3)

plot(qPrime,'-r','Linewidth',2)

title('Linear Power Change over Time','FontWeight','bold')

xlabel('Time (seconds)');

ylabel('Linear Power (W/cm)');

grid on

subplot(2,2,4)

plot(v/100,'Linewidth',2)

title('Moderator Velocity Change over Time','FontWeight','bold')

xlabel('Time (seconds)');

ylabel('Velocity (m/s)');

grid on

end

# Vita

Ian Stewart graduated from the University of Tennessee in Knoxville, TN in 2013 with a Bachelor of Science in Nuclear Engineering. Following graduation, Ian enrolled at the University of Tennessee to pursue his Doctorate in Nuclear Engineering. Upon completion of his Master’s degree under Dr. L.F. Miller, Ian will join Dr. Howard Hall’s group at the University of Tennessee for his Doctorate. His interests within the nuclear field have narrowed to nuclear safeguards/security and radiation transport. Ian’s professional goals are to work on an international level in nuclear security and non-proliferation.