## Slide 1: Temperature Dependent Mechanical Behavior of Solid Acids
Ryan Ginder

## Slide 2: Solid Acids – an introduction
Part 1

## Slide 3: Fuel Cell (FC) Operation
Harvests energy from water production
Classified by internal conducting layer material and operating temperature

## Slide 4: Solid Acid Use in FCs

## Slide 5: Solid Acids (Acid Salts)
Formed by only partially neutralizing acids
MHXO4, MH2ZO4, MHXO4 - MH2ZO4
  X = S, Se
  Z = P, As
  M = Li, Na, K, NH4, Rb, Cs
Cesium Hydrogen Sulfate (CHS)
CsHSO4

## Slide 6: CHS Superprotonic Transition
Phase III & Phase II (Sub-Superprotonic)
Phase I (Superprotonic)

## Slide 7: Superprotonic Phase Plasticity
Uniaxial Compression Testing
Fuel Cell Schematic
  2.5 x 3 x 10 mm specimens

## Slide 8: Time Dependent Deformation (Creep)
Secondary Creep
Log-Log Fitting
Start Time
Elastic Strain
Primary
Secondary
Tertiary
Steady State Regime

## Slide 9: Kislitsyn CHS Creep Tests
Uniaxially pressed powder to form thin disc specimens
Specimens deformed with fixed nominal stress
Sample
Furnace
LVDT
Linear Motor
Thermocouple
Thermomechanical Analyzer Schematic

## Slide 10: Kislitsyn CHS Results
Stress Exponent
Activation Energy
Chart: Flow Stress (MPa)
| 0.23275816590766188 | 0.32104093149644547 | 0.37556493006806979 | 0.40224398144252171
160 C | 3.5835e-06 | 7.2412e-06 | 1.0655e-05 | 1.1574e-05
120 C | 2.3047e-06 | 2.7009e-06 | 3.2989e-06 | 3.9467e-06 | 4.1995e-06
Chart: 1000/T (1000/K)
| 2.2822033898305083 | 2.336440677966102 | 2.3635593220338986 | 2.4211864406779662 | 2.4508474576271189 | 2.4813559322033902 | 2.5135593220338985 | 2.5449152542372886
CHS at 330 kPa | 2.4262e-05 | 1.8743e-05 | 1.1932e-05 | 6.209e-06 | 3.9527e-06 | 3.9847e-06 | 4.4251e-06 | 3.8894e-06
Superprotonic Transition | 0.0001 | 7.75e-05 | 5.5e-05 | 3.25e-05 | 1e-05 | 1.3e-05 | 1.6e-05 | 1e-06
2eV Fit | 2.4262e-05 | 1.8743e-05 | 1.1932e-05 | 6.209e-06
1eV Fit | 3.9527e-06 | 3.9847e-06 | 4.4251e-06 | 3.8894e-06
Superprotonic
Sub-superprotonic

## Slide 11: Small Strain & Aspect Ratio

## Slide 12: Another Approach Needed
Uniaxial compression unreliable for FC membrane specimens
Could make much larger compression test specimens
Or…nanoindentation can probe smaller volumes
But…nanoindentation needs interpretation

## Slide 13: References
[1] Dervisoglu, R. (2012). "Solid oxide fuel cell." 2016, from https://commons.wikimedia.org/wiki/File:Solid_oxide_fuel_cell_protonic.svg.
[2] Energy, U. S. D. o. (2015). "Comparison of Fuel Cell Technologies." 2016, from http://energy.gov/sites/prod/files/2015/06/f23/fcto_fuel_cells_comparison_chart.pdf.
[3] Duong, H. H. (2009). Solid Acid Fuel Cell Stack for APU Applications. 2009 DOE Hydrogen Program and Vehicle Technologies Program Annual Merit Review and Peer Evaluation Meeting. Washington, DC, U.S. Department of Energy: 1-30.
[4] Chisholm, C. R. I. (2003). Superprotonic Phase Transitions in Solid Acids: Parameters affecting the presence and stability of superprotonic transitions in the MHnXO4 family of compounds (X=S, SE, P, AS; M=Li, Na, K, NH4, Rb, Cs). Materials Science. Pasadena, CA, California Institute of Technology. Ph. D.: 290.
[5] Mhiri, T., et al. (1992). "SUPERPROTONIC PHASE-TRANSITION IN MIXED AMMONIUM CESIUM ACID SULFATE CS0.9(NH4)0.1HSO4." Journal of Alloys and Compounds 188(1-2): 215-220.
[6] Baranov, A. I., et al. (1982). "SUPERION CONDUCTIVITY AND PHASE-TRANSITIONS IN CSHSO4 AND CSHSEO4 CRYSTALS." Jetp Letters 36(11): 459-462.
[7] Haile, S. M., et al. (2001). "Solid acids as fuel cell electrolytes." Nature 410(6831): 910-913.
[8] Ozaki, T., et al. (1982). "PLASTIC-DEFORMATION BY TWINNING IN CSHSO4 SINGLE-CRYSTAL." Journal of the Physical Society of Japan 51(1): 213-218.
[9] Kirpichnikova, L. F., et al. (1995). "SUPERPLASTICITY OF CSHSO4 CRYSTALS IN THE SUPERIONIC PHASE." Jetp Letters 62(8): 638-641.
[10] Strafpeloton2 (2009). "3StageCreep." 2016, from https://commons.wikimedia.org/wiki/File:3StageCreep.svg.
[11] Cjp24 (2008). "Thermomechanical analyzer." 2016, from https://commons.wikimedia.org/wikiFile:Thermomechanical_analyzer.png.
[12] Kislitsyn, M. N. (2009). Materials Chemistry of Superprotonic Acids. Materials Science. Pasadena, CA, California Institute of Technology. Ph. D.: 181.

## Slide 14: The Characterization of Steady State Creep via Nanoindentation
Part 2

## Slide 15: Nanoindentation
Device Basics
  Input: Load → Output: Displacement
  Calibrate with area function
  Calculate hardness
Probe tip typically Berkovich geometry
  Minimize friction
  Axisymmetric indenter

## Slide 16: Time-Independent Models
Oliver & Pharr Method
Hardness & Young’s Modulus
Based on Sneddon’s elastic theory
Johnson Cavity Model
Yield Strength & Deformation Regime
Based on Hill elastic-perfectly plastic expanding cavity

## Slide 17: Mechanical Testing
Uniaxial Compression
Nanoindentation

## Slide 18: Compression vs. Indentation
Uniaxial
→ uniaxial creep rate
→ uniaxial pre-exponential
→ true flow stress
→ uniaxial stress exponent
Indentation
→ indentation creep rate
→ indentation pre-exponential
→ contact stress (hardness)
→ stress exponent

## Slide 19: Impression Creep
Chu & Li showed steady state creep via cylindrical flat punch
Derived empirical equation for power law creep behavior:

## Slide 20: Hill: Elastic-Perfectly Plastic Cavity
Cavity Formation & Growth

## Slide 21: Johnson: Expanding Cavity Model (ECM)

## Slide 22: Johnson: ECM

## Slide 23: Johnson Relation
Cavity to Indenter Connection

## Slide 24: Elastic-Perfectly Plastic ECM
Elastic-Plastic Deformation Regime

## Slide 25: Building Towards Creep
not elastic-plastic specific
I’ve adapted for steady state creep indentation
Need creeping cavity description from Finnie & Heller for gas bubbles in fission materials

## Slide 26: Steady-State, Multiaxial Stress Creep
Von Mises criterion
Principal axes of strain do not rotate during creep
Volume is conserved during plastic deformation
Stressed body’s mechanical properties are isotropic
Principal shear-strain rates are proportional to principle shear stresses by a constant

## Slide 27: Creeping Spherical Pressure Vessel in Infinite Medium

## Slide 28: My Creep Indentation Model
General Form
Conical (Berkovich) Indentation
*Set

## Slide 29: Bower’s Analysis
Nonlinear Creep Law
Indentation Creep
Conical (Berkovich) Indentation

## Slide 30: Tabulated Bower Coefficients
1/n | c, Cone | c, Sphere | F
1 | 0.636 | 0.707 | 0.849
0.9 | 0.692 | 0.747 | 1.085
0.8 | 0.745 | 0.788 | 1.332
0.7 | 0.802 | 0.831 | 1.602
0.6 | 0.859 | 0.875 | 1.886
0.5 | 0.916 | 0.92 | 2.176
0.4 | 0.974 | 0.966 | 2.465
0.3 | 1.033 | 1.013 | 2.734
0.2 | 1.097 | 1.065 | 2.973
0.1 | 1.174 | 1.128 | 3.11
0.01 | 1.263 | 1.201 | 3.051
Chart: Fitted Bower Parameters
| 1 | 0.9 | 0.8 | 0.70000000000000007 | 0.60000000000000009 | 0.50000000000000011 | 0.40000000000000013 | 0.30000000000000016 | 0.20000000000000015 | 0.10000000000000014 | 0.01
F | 0.849 | 1.085 | 1.332 | 1.602 | 1.886 | 2.176 | 2.465 | 2.734 | 2.973 | 3.11 | 3.051
c, Cone | 0.636 | 0.692 | 0.745 | 0.802 | 0.859 | 0.916 | 0.974 | 1.033 | 1.097 | 1.174 | 1.263
c, Sphere | 0.707 | 0.747 | 0.788 | 0.831 | 0.875 | 0.92 | 0.966 | 1.013 | 1.065 | 1.128 | 1.201

## Slide 31: Chu & Li Experiments
Flat Punch Indent Data
Uniaxial Compression Data

## Slide 32: Flat Punch Results
Nonlinear creep law appears to work
My model suggests for radial flow dominates indent creep
Chart: Succinonitrile Crystal Steady State Creep
| 32394.494261605909 | 33385.678696871742 | 46044.341389004207 | 64791.543281486294
Uniaxial | 1.2735e-06 | 1.6596e-06 | 5.6234e-06 | 1.7579e-05
Indentation | 6.0968e-05 | 0.00012061 | 0.00021221 | 0.00035399 | 6.4988e-05 | 0.0001272 | 0.00024373 | 0.00039377 | 6.3052e-05 | 0.00012474 | 0.00022182 | 0.00037398 | 6.7295e-05 | 0.00012894 | 0.00024971 | 0.00041212 | 6.0283e-05 | 0.00011799 | 0.00022131 | 0.00036139
My Model | 6.0968e-05 | 0.00012061 | 0.00021221 | 0.00035399 | 6.4988e-05 | 0.0001272 | 0.00024373 | 0.00039377 | 6.3052e-05 | 0.00012474 | 0.00022182 | 0.00037398 | 6.7295e-05 | 0.00012894 | 0.00024971 | 0.00041212 | 6.0283e-05 | 0.00011799 | 0.00022131 | 0.00036139
Bower | 6.0968e-05 | 0.00012061 | 0.00021221 | 0.00035399 | 6.4988e-05 | 0.0001272 | 0.00024373 | 0.00039377 | 6.3052e-05 | 0.00012474 | 0.00022182 | 0.00037398 | 6.7295e-05 | 0.00012894 | 0.00024971 | 0.00041212 | 6.0283e-05 | 0.00011799 | 0.00022131 | 0.00036139
Uni Fit | 1e-06 | 1e-05 | 0.0001 | 0.001
Ind Fit | 1e-06 | 1e-05 | 0.0001 | 0.001

## Slide 33: Su: Amorphous Selenium Experiments
Berkovich Indent Data
Uniaxial Compression Data

## Slide 34: Berkovich Results
Nonlinear creep law still works for conical/Berkovich indents
Again radial flow dominates, now at
Chart: Amorphous Selenium Steady State Creep
| 8743999.8147397153 | 1180714.569697462 | 159433.54581799684
Uniaxial | 0.0001 | 1e-05 | 1e-06
Indentation | 0.0001 | 1e-05 | 1e-06 | 5e-05 | 5e-06
My model | 0.0001 | 1e-05 | 1e-06 | 5e-05 | 5e-06
Bower | 0.0001 | 1e-05 | 1e-06 | 5e-05 | 5e-06

## Slide 35: High Purity Indium:

## Slide 36: Indium Results Comparison
Experiments done by different folks 40 years apart
Suggests radial flow still dominate at
Chart: High Purity Indium Steady State Creep
| 2400000 | 1400000 | 1800000
Uniaxial | 0.0026667 | 4.3333e-05 | 0.00013333
Indentation | 0.0025102 | 0.0049024 | 0.0051548 | 0.0097358 | 0.010067 | 0.046937 | 0.049353 | 0.090145 | 0.098012
My model | 0.0025102 | 0.0049024 | 0.0051548 | 0.0097358 | 0.010067 | 0.046937 | 0.049353 | 0.090145 | 0.098012
Bower | 0.0025102 | 0.0049024 | 0.0051548 | 0.0097358 | 0.010067 | 0.046937 | 0.049353 | 0.090145 | 0.098012
Uni Fit | 1e-05 | 0.0001 | 0.001 | 0.01 | 0.1 | 1
Ind Fit | 1e-05 | 0.0001 | 0.001 | 0.01 | 0.1 | 1

## Slide 37: Parameter
Bower Analysis
My Model

## Slide 38: Comparison
Radial flow dominate
Peak occurs around where Bower
Peak possibly indicates shift in surface flow
Chart: α/β Parameter Ratio

## Slide 39: Measurement & Analysis of Superprotonic CHS Mechanical Properties
Part 3

## Slide 40: Raw CHS Synthesis/Processing
CHS powder synthesized via aqueous chemistry
Powder precipitated, hand ground, & thoroughly dried
Powder kept stored at 110°C under ambient air

## Slide 41: CHS Thermodynamic Stability
Solid acids can convert to dehydrant phases
CHS robust against this
Samples tested for safe timeframes

## Slide 42: Compressive Creep Testing
MTS10/GL screw driven uniaxial tension & compression load frame
Temperature set by environmental chamber
Constant & variable displacement rate (CDR & VDR) tests

## Slide 43: Uniaxial Sample Fabrication
CHS powder pressed uniaxially in compression die
Pressed under 125 MPa (18 ksi) for 20 minutes
Aspect ratios of ~2.5
Densities are ~96-99% of theoretical density

## Slide 44: Sub-Superprotonic:
Chart: True Strain (%)

## Slide 45: Sub-superprotonic Deformation
Double Barreling
Cracking

## Slide 46: Superprotonic CHS CDR Data Initial
Chart: Strain Rate Variation, T = 160°C
Chart: Temperature Variation, Strain Rate = 10^-4

## Slide 47: CDR Data Initial - Analysis

## Slide 48: Superprotonic CHS VDR Data
Chart: CHS VDR 150°C
Chart: CHS VDR 160°C
Chart: CHS VDR 145°C
Experimental Conditions
from 0-3% strain
from 3-6% strain
from 6-10% strain
from 10-20% strain
*strain = total engineering strain

## Slide 49: Uniaxial VDR Creep Analysis
Chart: VDR Results - CHS Steady State Creep
| 6.4462522800000004 | 6.7137528499999997 | 6.0123749699999998 | 3.7015368000000004 | 3.9288586999999993 | 3.5180179199999997 | 2.0869401600000002 | 2.27806906 | 2.0153449999999999 | 1.0102176299999999 | 1.18975944 | 0.99181012000000002
160 C | 0.012946 | 0.01208 | 0.012328 | 0.0012157 | 0.00099459 | 0.0011051 | 0.00010618 | 0.00010618 | 0.00010618 | 1.2881e-05 | 9.6604e-06 | 9.6602e-06
150 C | 0.012203 | 0.012203 | 0.01208 | 0.00099459 | 0.0011051 | 0.0011051 | 0.00010618 | 0.00010618 | 0.00010618 | 9.6603e-06 | 9.6602e-06 | 9.6603e-06
145 C | 0.012089 | 0.012211 | 0.012087 | 0.0011052 | 0.0011052 | 0.0011051 | 0.00010618 | 0.00010618 | 0.00010618 | 9.6602e-06 | 1.288e-05 | 9.6602e-06
Chart: VDR Results Power Law Fit
| 8.5280406000000006 | 8.7205847500000004 | 8.6275169999999992 | 4.9763999999999999 | 5.0967384000000004 | 5.0370772700000002 | 2.9505340800000002 | 3.0165213399999997 | 3.0042781999999999 | 1.6798662600000001 | 1.70506308 | 1.6818071800000001
145 C | 1.0161e+23 | 1.0263e+23 | 1.016e+23 | 9.289e+21 | 9.289e+21 | 9.2889e+21 | 8.9248e+20 | 8.9246e+20 | 8.9246e+20 | 8.1196e+19 | 1.0826e+20 | 8.1196e+19
150 C | 5.206e+22 | 5.206e+22 | 5.1535e+22 | 4.2431e+21 | 4.7145e+21 | 4.7145e+21 | 4.5299e+20 | 4.53e+20 | 4.5298e+20 | 4.1212e+19 | 4.1212e+19 | 4.1212e+19
160 C | 1.4912e+22 | 1.3915e+22 | 1.42e+22 | 1.4003e+21 | 1.1457e+21 | 1.273e+21 | 1.2231e+20 | 1.2231e+20 | 1.2231e+20 | 1.4837e+19 | 1.1128e+19 | 1.1127e+19

## Slide 50: Superprotonic CDR Data Full
Chart: CHS CDR 145°C
Chart: CHS CDR 150°C
Chart: CHS CDR 160°C
Experimental Conditions
Tests run from 0-10% total engineering strain
Nominal strain rates of , , , tested

## Slide 51: Uniaxial CDR Creep Analysis
Chart: CDR Results - CHS Steady State Creep
| 8.6939025600000015 | 8.4472128000000009 | 7.8428063999999997 | 4.9579751999999999 | 4.6875097499999994 | 4.4816360999999993 | 2.4963983799999996 | 2.4176523200000002 | 2.3714283800000002 | 1.27668691 | 1.3038168000000001 | 1.32376629
160 C | 0.009214 | 0.0092051 | 0.0092051 | 0.001228 | 0.001228 | 0.0012281 | 0.00011334 | 0.00010915 | 0.00012043 | 1.1224e-05 | 1.0328e-05 | 1.0328e-05
150 C | 0.011045 | 0.011043 | 0.011047 | 0.0011603 | 0.001105 | 0.0011603 | 0.00011742 | 0.00011051 | 0.0001105 | 1.0361e-05 | 1.1224e-05 | 1.1223e-05
145 C | 0.011048 | 0.011047 | 0.011156 | 0.001105 | 0.001105 | 0.001105 | 0.0001105 | 0.0001105 | 0.00011051 | 1.1223e-05 | 1.1224e-05 | 1.1224e-05
Chart: CDR Results Power Law Fit
| 11.221402640000001 | 10.68077014 | 10.144729719999999 | 6.6537297000000004 | 7.2088602799999997 | 7.1388349900000003 | 3.43763912 | 3.3109925099999997 | 3.3171434399999997 | 1.7066225399999999 | 1.6386471300000001 | 1.6602713
145 C | 24444711642.8258 | 24443901490.8151 | 24684931750.1876 | 2444903097.2565 | 2445065201.0281 | 2444876082.051 | 244501116.0466 | 244498414.2874 | 244511923.6813 | 24832281.7775 | 24833928.3077 | 24835300.5829
150 C | 17465900864.6755 | 17463779179.599 | 17469566807.9578 | 1834861749.5395 | 1747419796.6519 | 1834963133.7594 | 185684896.9744 | 174761290.2625 | 174743910.3024 | 16384595.2125 | 17749291.6009 | 17748507.0368
160 C | 7618231852.3427 | 7610826522.1826 | 7610826522.1826 | 1015292659.9182 | 1015281439.3555 | 1015393656.1493 | 93713108.1943 | 90243249.6084 | 99574028.8447 | 9280050.4873 | 8539656.0257 | 8539372.9088

## Slide 52: CHS Activation Energy
Self-diffusion known for monoclinic phase at 120°C
For deuterated CHS
  = 0.70 +/- 0.03 eV
  = 0.60 +/- 0.02eV
Q = 1.03 eV seems reasonable result
120°C Self Diffusion Energies

## Slide 53: Indentation Specimen Polishing
CHS is both soft and water soluble!
Final Preparation Procedure
Ground on SiC P1500, P2500, & P4000 grit papers by hand
Specimens sonicated clean in anhydrous toluene
Samples put on vibratory polisher for at least 24hrs in mineral oil/alumina microparticle slurry

## Slide 54: Area Function
Chart: Berkovich Diamond Tip Area Function

## Slide 55: Nanoindentation Test Methods
Constant Strain Rate (CSR) Tests
For isotropic, homogenous materials with constant bulk hardness, constant yields constant
When contact pressure (i.e. hardness) becomes constant, specimen deforming in steady state regime

## Slide 56: CSR 145°C Data
Load
Hardness

## Slide 57: CSR 150°C Data
Load
Hardness

## Slide 58: CSR 160°C Data
Load
Hardness

## Slide 59: CSR Stress Exponent Results

## Slide 60: CSR Activation Energy
Chart: Indentation Results Power Law Fit
| 47.599148395206839 | 46.395438566468357 | 51.261134234521478 | 30.198320728912211 | 21.581786487988627 | 25.788337984067013 | 19.526379096972263 | 16.786259340251984 | 15.964760362852388 | 14.797205372916427
145 C | 443735876637.375 | 392576811192.526 | 405184755895.2797 | 66990822706.0745 | 66743213404.503 | 59086801593.6328 | 56954190819.9552 | 4704505531.3017 | 5696193412.7397 | 6064747337.1829
150 C | 435504560940.244 | 585523997888.6558 | 616507130860.3308 | 47286882174.8258 | 48697412598.1398 | 51001778705.2475 | 49214670517.1273 | 4255524189.5115 | 4158007016.7559
160 C | 245762853980.9905 | 232641938854.9352 | 217479363045.0178 | 17079645253.4417 | 21649139928.1748 | 17313088797.567 | 3700215716.2683 | 4556302377.3284 | 3038313774.4103
Chart: Full Results Power Law Fit
| 11.221402640000001 | 10.68077014 | 10.144729719999999 | 6.6537297000000004 | 7.2088602799999997 | 7.1388349900000003 | 3.43763912 | 3.3109925099999997 | 3.3171434399999997 | 1.7066225399999999 | 1.6386471300000001 | 1.6602713 | 8.0610273599999989 | 8.6756175800000008 | 8.5089856499999996 | 5.1666934999999992 | 4.6448003699999996 | 5.4441816000000003 | 2.6736840000000002 | 2.4827986400000004 | 2.0550278999999998 | 1.3589945800000001 | 1.7354447599999998 | 1.61427024 | 8.6939025600000015 | 8.4472128000000009 | 7.8428063999999997 | 4.9579751999999999 | 4.6875097499999994 | 4.4816360999999993 | 2.4963983799999996 | 2.4176523200000002 | 2.3714283800000002 | 1.27668691 | 1.3038168000000001 | 1.32376629
Uniaxial | 24444711642.8258 | 24443901490.8151 | 24684931750.1876 | 2444903097.2565 | 2445065201.0281 | 2444876082.051 | 244501116.0466 | 244498414.2874 | 244511923.6813 | 24832281.7775 | 24833928.3077 | 24835300.5829 | 17465900864.6755 | 17463779179.599 | 17469566807.9578 | 1834861749.5395 | 1747419796.6519 | 1834963133.7594 | 185684896.9744 | 174761290.2625 | 174743910.3024 | 16384595.2125 | 17749291.6009 | 17748507.0368 | 7618231852.3427 | 7610826522.1826 | 7610826522.1826 | 1015292659.9182 | 1015281439.3555 | 1015393656.1493 | 93713108.1943 | 90243249.6084 | 99574028.8447 | 9280050.4873 | 8539656.0257 | 8539372.9088
Indentation | 443735876637.375 | 392576811192.526 | 405184755895.2797 | 66990822706.0745 | 66743213404.503 | 59086801593.6328 | 56954190819.9552 | 4704505531.3017 | 5696193412.7397 | 6064747337.1829 | 435504560940.244 | 585523997888.6558 | 616507130860.3308 | 47286882174.8258 | 48697412598.1398 | 51001778705.2475 | 49214670517.1273 | 4255524189.5115 | 4158007016.7559 | 245762853980.9905 | 232641938854.9352 | 217479363045.0178 | 17079645253.4417 | 21649139928.1748 | 17313088797.567 | 3700215716.2683 | 4556302377.3284 | 3038313774.4103
My model | 443735876637.375 | 392576811192.526 | 405184755895.2797 | 66990822706.0745 | 66743213404.503 | 59086801593.6328 | 56954190819.9552 | 4704505531.3017 | 5696193412.7397 | 6064747337.1829 | 435504560940.244 | 585523997888.6558 | 616507130860.3308 | 47286882174.8258 | 48697412598.1398 | 51001778705.2475 | 49214670517.1273 | 4255524189.5115 | 4158007016.7559 | 245762853980.9905 | 232641938854.9352 | 217479363045.0178 | 17079645253.4417 | 21649139928.1748 | 17313088797.567 | 3700215716.2683 | 4556302377.3284 | 3038313774.4103
Bower | 443735876637.375 | 392576811192.526 | 405184755895.2797 | 66990822706.0745 | 66743213404.503 | 59086801593.6328 | 56954190819.9552 | 4704505531.3017 | 5696193412.7397 | 6064747337.1829 | 435504560940.244 | 585523997888.6558 | 616507130860.3308 | 47286882174.8258 | 48697412598.1398 | 51001778705.2475 | 49214670517.1273 | 4255524189.5115 | 4158007016.7559 | 245762853980.9905 | 232641938854.9352 | 217479363045.0178 | 17079645253.4417 | 21649139928.1748 | 17313088797.567 | 3700215716.2683 | 4556302377.3284 | 3038313774.4103
Uni Fit | 1000000 | 10000000000000
Ind Fit | 1000000 | 10000000000000

## Slide 61: Full Creep Comparison
Chart: True Flow Stress (MPa)
| 0.23275816590766188 | 0.32104093149644547 | 0.37556493006806979 | 0.40224398144252171
Kislitsyn 160 C | 6.6778e+17 | 1.3494e+18 | 1.9855e+18 | 2.1568e+18
Uniaxial - CDR | 24444711642.8258 | 24443901490.8151 | 24684931750.1876 | 2444903097.2565 | 2445065201.0281 | 2444876082.051 | 244501116.0466 | 244498414.2874 | 244511923.6813 | 24832281.7775 | 24833928.3077 | 24835300.5829 | 17465900864.6755 | 17463779179.599 | 17469566807.9578 | 1834861749.5395 | 1747419796.6519 | 1834963133.7594 | 185684896.9744 | 174761290.2625 | 174743910.3024 | 16384595.2125 | 17749291.6009 | 17748507.0368 | 7618231852.3427 | 7610826522.1826 | 7610826522.1826 | 1015292659.9182 | 1015281439.3555 | 1015393656.1493 | 93713108.1943 | 90243249.6084 | 99574028.8447 | 9280050.4873 | 8539656.0257 | 8539372.9088
Uniaxial - VDR | 1.0161e+23 | 1.0263e+23 | 1.016e+23 | 9.289e+21 | 9.289e+21 | 9.2889e+21 | 8.9248e+20 | 8.9246e+20 | 8.9246e+20 | 8.1196e+19 | 1.0826e+20 | 8.1196e+19 | 5.206e+22 | 5.206e+22 | 5.1535e+22 | 4.2431e+21 | 4.7145e+21 | 4.7145e+21 | 4.5299e+20 | 4.53e+20 | 4.5298e+20 | 4.1212e+19 | 4.1212e+19 | 4.1212e+19 | 1.4912e+22 | 1.3915e+22 | 1.42e+22 | 1.4003e+21 | 1.1457e+21 | 1.273e+21 | 1.2231e+20 | 1.2231e+20 | 1.2231e+20 | 1.4837e+19 | 1.1128e+19 | 1.1127e+19
Indentation | 443735876637.375 | 392576811192.526 | 405184755895.2797 | 66990822706.0745 | 66743213404.503 | 59086801593.6328 | 56954190819.9552 | 4704505531.3017 | 5696193412.7397 | 6064747337.1829 | 435504560940.244 | 585523997888.6558 | 616507130860.3308 | 47286882174.8258 | 48697412598.1398 | 51001778705.2475 | 49214670517.1273 | 4255524189.5115 | 4158007016.7559 | 245762853980.9905 | 232641938854.9352 | 217479363045.0178 | 17079645253.4417 | 21649139928.1748 | 17313088797.567 | 3700215716.2683 | 4556302377.3284 | 3038313774.4103
My model | 443735876637.375 | 392576811192.526 | 405184755895.2797 | 66990822706.0745 | 66743213404.503 | 59086801593.6328 | 56954190819.9552 | 4704505531.3017 | 5696193412.7397 | 6064747337.1829 | 435504560940.244 | 585523997888.6558 | 616507130860.3308 | 47286882174.8258 | 48697412598.1398 | 51001778705.2475 | 49214670517.1273 | 4255524189.5115 | 4158007016.7559 | 245762853980.9905 | 232641938854.9352 | 217479363045.0178 | 17079645253.4417 | 21649139928.1748 | 17313088797.567 | 3700215716.2683 | 4556302377.3284 | 3038313774.4103
Bower | 443735876637.375 | 392576811192.526 | 405184755895.2797 | 66990822706.0745 | 66743213404.503 | 59086801593.6328 | 56954190819.9552 | 4704505531.3017 | 5696193412.7397 | 6064747337.1829 | 435504560940.244 | 585523997888.6558 | 616507130860.3308 | 47286882174.8258 | 48697412598.1398 | 51001778705.2475 | 49214670517.1273 | 4255524189.5115 | 4158007016.7559 | 245762853980.9905 | 232641938854.9352 | 217479363045.0178 | 17079645253.4417 | 21649139928.1748 | 17313088797.567 | 3700215716.2683 | 4556302377.3284 | 3038313774.4103
VDR Fit | 1000000000000 | 10000000000000000 | 1e+20 | 1e+24
CDR Fit | 1000 | 1000000 | 1000000000 | 1000000000000 | 10000000000000000

## Slide 62: CSR Young’s Modulus
Chart: Average Young's Modulus
| 145 | 150 | 160
Superprotonic | 7.7468 | 4.4126 | 4.2533
Sub-superprotonic | 22
Superprotonic Transition
Chart: RT Modulus
145°C
150°C
160°C

## Slide 63: References

## Slide 64: Final Conclusions
Part 4

## Slide 65: Solid Acid Creep Behavior
Creep appears to be a serious problem under compressive loading for CHS.
Stress exponent and activation energy consistent with a dislocation based creep mechanism, contrary to the results of Kislitsyn.
Elastic modulus is also low after transition resulting in large time-independent deformation as well.

## Slide 66: Indentation Measured Creep
My model does provide a relatively simple, closed form description for indentation steady state creep.
My model’s approximation of indentation creep compares well with Bower’s finite element/numerically augmented model which work for reasonably large range of stress exponent.
Nanoindentation can successfully probe both time-independent and time-dependent properties simultaneously using small volumes.

## Slide 67: Acknowledgements
Adviser
Group members
ChemE folks
NMI staff
Now defunct TN-SCORE, Bredesen Center, & NDSEG (DoD)

## Slide 68
145°C:
150°C:
Chart: Flow Stress or Hardness (MPa)
| 11.221402640000001 | 10.68077014 | 10.144729719999999 | 6.6537297000000004 | 7.2088602799999997 | 7.1388349900000003 | 3.43763912 | 3.3109925099999997 | 3.3171434399999997 | 1.7066225399999999 | 1.6386471300000001 | 1.6602713
Uniaxial | 0.011048 | 0.011047 | 0.011156 | 0.001105 | 0.001105 | 0.001105 | 0.0001105 | 0.0001105 | 0.00011051 | 1.1223e-05 | 1.1224e-05 | 1.1224e-05
Indentation | 0.071203 | 0.062994 | 0.065017 | 0.010749 | 0.01071 | 0.0094812 | 0.009139 | 0.00075489 | 0.00091402 | 0.00097316
My model | 0.071203 | 0.062994 | 0.065017 | 0.010749 | 0.01071 | 0.0094812 | 0.009139 | 0.00075489 | 0.00091402 | 0.00097316
Bower | 0.071203 | 0.062994 | 0.065017 | 0.010749 | 0.01071 | 0.0094812 | 0.009139 | 0.00075489 | 0.00091402 | 0.00097316
Uni Fit | 1e-05 | 1
Ind Fit | 1e-05 | 1
Chart: Flow Stress or Hardness (MPa)
| 8.0610273599999989 | 8.6756175800000008 | 8.5089856499999996 | 5.1666934999999992 | 4.6448003699999996 | 5.4441816000000003 | 2.6736840000000002 | 2.4827986400000004 | 2.0550278999999998 | 1.3589945800000001 | 1.7354447599999998 | 1.61427024
Uniaxial | 0.011045 | 0.011043 | 0.011047 | 0.0011603 | 0.001105 | 0.0011603 | 0.00011742 | 0.00011051 | 0.0001105 | 1.0361e-05 | 1.1224e-05 | 1.1223e-05
Indentation | 0.09898 | 0.13308 | 0.14012 | 0.010747 | 0.011068 | 0.011592 | 0.011185 | 0.00096718 | 0.00094502
My model | 0.09898 | 0.13308 | 0.14012 | 0.010747 | 0.011068 | 0.011592 | 0.011185 | 0.00096718 | 0.00094502
Bower | 0.09898 | 0.13308 | 0.14012 | 0.010747 | 0.011068 | 0.011592 | 0.011185 | 0.00096718 | 0.00094502
Uni Fit | 1e-05 | 1
Ind Fit | 1e-05 | 1

## Slide 69
160°C:
Chart: Flow Stress or Hardness (MPa)
| 8.6939025600000015 | 8.4472128000000009 | 7.8428063999999997 | 4.9579751999999999 | 4.6875097499999994 | 4.4816360999999993 | 2.4963983799999996 | 2.4176523200000002 | 2.3714283800000002 | 1.27668691 | 1.3038168000000001 | 1.32376629
Uniaxial | 0.009214 | 0.0092051 | 0.0092051 | 0.001228 | 0.001228 | 0.0012281 | 0.00011334 | 0.00010915 | 0.00012043 | 1.1224e-05 | 1.0328e-05 | 1.0328e-05
Indentation | 0.10939 | 0.10355 | 0.096798 | 0.007602 | 0.0096359 | 0.0077059 | 0.0016469 | 0.002028 | 0.0013523
My model | 0.10939 | 0.10355 | 0.096798 | 0.007602 | 0.0096359 | 0.0077059 | 0.0016469 | 0.002028 | 0.0013523
Bower | 0.10939 | 0.10355 | 0.096798 | 0.007602 | 0.0096359 | 0.0077059 | 0.0016469 | 0.002028 | 0.0013523
Uni Fit | 1e-05 | 1
Ind Fit | 1e-05 | 1